Division 03

Section: 03 05 53 – Concrete Admixtures

Specification Language

#### Alkali-Silica Reaction Inhibiting Admixture: (ASTM C 494/C 494M / AASHTO M 194 M/M 194: Type S)

#### Shall contain a nominal lithium nitrate content of 30 percent.

#### Shall meet the requirements of ASTM C 494 / AASHTO M 194: Type S: [MasterLife ASR 30 (formerly ASRx 30 LN)] by BASF Corporation