SECTION 07 19 16

MasterProtect® H 1000 Sealer (Formerly Hydrozo 100)

Notes to specifiers:

Please update your Master Specifications to reflect the company and product name changes. The old product names are provided in parentheses following the new names in this Section for reference.

The purpose of this guide specification is to assist the specifier in developing a project specification for the use of master buidlers solutions products.  this guide document has been prepared to be part of a complete project manual.  it is not intended to be a “stand alone” document, and it is not intended to be copied directly into a project manual.

This guide specification will need to be carefully reviewed for APPROPRIATENESS for the given project and edited accordingly to comply with project-specific requirements.

GENERAL

SUMMARY

Section Includes:

edit note:  Delete application not required.

Water repellent sealer for interior or exterior concrete surfaces as scheduled.

edit note:  Delete sections below not relevant to this project; add others as required.

Related Sections:

Section 03 30 00 – Cast-in-Place Concrete.

Section 03 41 00 – Precast Structural Concrete.

Section 04 21 00 – Masonry Assemblies Unit Masonry.

Section 09 24 00 – Portland Cement Plastering.

Section 09 30 19 – Paver Tiling.

Section 09 31 33 – Thin-Set Stone Tiling.

SUBMITTALS

Comply with Section [01 33 00] [__ __ __].

Product Data:  Submit manufacturer's technical data sheets.

LEED Submittals:  Comply with requirements for each product to achieve points indicated in LEED Project Checklist provided by the architect/engineer.

Submit list of project references as documented in this specification under Quality Assurance Article.  Include contact name and phone number of the person charged with oversight of each project.

Quality Control Submittals:

Provide protection plan of surrounding areas and non-work surfaces.

QUALITY ASSURANCE

Comply with Section [01 40 00] [__ __ __].

Qualifications:

Manufacturer Qualifications:  Company with minimum 15 years of experience in manufacturing of specified products.

Manufacturer Qualifications:  Company shall be ISO 9001:2015 Certified.

Applicator Qualifications:  Company with minimum of 5 years’ experience in application of specified products on projects of similar size and scope and is acceptable to product manufacturer.

Successful completion of a minimum of 5 projects of similar size and complexity to specified work.

Field Sample:

Install field sample at project site or other pre-selected area, as directed by architect/engineer.

Provide mockup of at least 100 sf (9.3 m2) to include surface preparation, sealant joint, and juncture details and allow for evaluation of repellent performance and finish.

Conduct absorption test on cured field sample.  Adjust application until required repellent performance is achieved.

Apply material in accordance with manufacturer’s written application instructions.

Manufacturer’s representative or designated representative will review technical aspects; surface preparation, application and workmanship.

Field sample will be standard for judging workmanship on remainder of project.

Maintain field sample during construction for workmanship comparison.

Do not alter, move, or destroy field sample until work is completed and approved by architect/engineer.

Obtain architect/engineer written approval of field sample before start of material application, including approval of aesthetics, color, texture, and appearance.

DELIVERY, STORAGE, AND HANDLING

Comply with Section [01 60 00] [__ __ __].

Comply with manufacturer’s ordering instructions and lead-time requirements to avoid construction delays.

Deliver materials in manufacturer's original, unopened, undamaged containers with identification labels intact.

Store in unopened containers in clean, dry area between 35 degrees F (2 degrees C) and 110 degrees F (43 degrees C).

PROJECT CONDITIONS

Environmental Requirements:

Minimum application temperature is 20 degrees F (minus 7 degrees C) and rising.

Do not apply in rain or when rain is expected within 4 hours.  Do not apply above 95 degrees F (35 degrees C) or below 40 degrees F (4 degrees C) or when temperatures are expected to fall below 20 degrees F (minus 7 degrees C) within 12 hours.

PRODUCTS

MANUFACTURERs

Subject to compliance with requirements, provide products from the following manufacturer:

Master Builders Solutions

889 Valley Park Drive

Shakopee, MN  55379 USA

Customer Service:  800-433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Website: www.master-builders-solutions.com/en-us

Substitutions:  Comply with Section [01 60 00] [__ __ __].

Specifications and drawings are based on manufacturer's proprietary literature from Master Builders Solutions.  Other manufacturers shall comply with minimum levels of material and detailing indicated in specifications or on drawings.  Architect/engineer will be sole judge of appropriateness of substitutions.

MATERIALS

Clear, breathable, high-performance, 100 percent silane sealer for protecting new and existing concrete surfaces.  Penetrates deeply, sealing out water, chloride ions, and acids, preventing damage from freeze/thaw cycles.

Acceptable Product:  MasterProtect H 1000 (formerly Hydrozo 100) by Master Builders Solutions.

Water repellant sealer complies with the following requirements:

Compliance:  Alberta DOT, Type 1c.

Silane Content by Weight:  100 percent.

Penetration, average depth, depending upon substrate:  0.35 inch (9 mm).

Surface Appearance after Application:  Unchanged.

Flash Point, SETA:  Greater than 165 degrees F (62.7 degrees C).

Waterproofing Repellency after Heavy Abrasion, Alberta DOT penetrating sealer, Type 1c, 0.35 w/c ratio:  83.5 percent.

Water Weight Gain, NCHRP 244 Series II Cube Test:

250 sf per gal (6.1 m2/L):  90 percent reduction.

400 sf per gal (9.8 m2/L):  85 percent reduction.

Absorbed Chloride, NCHRP 244 Series II Cube Test:

250 sf per gal (6.1 m2/L):  96 percent reduction.

400 sf per gal (9.8 m2/L):  87 percent reduction.

Absorbed Chloride, NCHRP 244 Series IV Southern Climate:  98 percent reduction.

VOC Content:

3.05 lbs per gal (365 g/L), less water and exempt solvents.

eXECUTION

EXAMINATION

Comply with Section [01 70 00] [__ __ __].

SURFACE PREPARATION

Protection:  Protect plant life and surfaces to remain uncoated during application.  Use drop cloths or masking as required.

Prepare surfaces in accordance with manufacturer’s instructions.

edit note:  Surface cleanliness is critical for blemish or stain-free results, especially on light colored or white surfaces.  Concrete should be cured to 80% of design strength prior to application of Sealer.

Verify substrate has properly cured.  Surfaces shall be clean and structurally sound.  Remove dust, dirt, oil, grease, chemical films, coatings and other contaminants before application.

Do not apply sealer if standing water is visible on surface to be treated.

application

Apply sealer in accordance with manufacturer’s instructions.

Stir material thoroughly before and during application.

Apply sealer with flooding action.  Eliminate ponding.

Apply even distribution of sealer.

PROTECTION

Protect sealer from damage during construction.

END OF SECTION

Disclaimer:

THIS INFORMATION AND ALL FURTHER TECHNICAL ADVICE ARE BASED ON master builders solutions PRESENT KNOWLEDGE AND EXPERIENCE. HOWEVER, master builders solutions ASSUMES NO LIABILITY FOR PROVIDING SUCH INFORMATION AND ADVICE INCLUDING THE EXTENT TO WHICH SUCH INFORMATION AND ADVICE MAY RELATE TO EXISTING THIRD-PARTY INTELLECTUAL PROPERTY RIGHTS, ESPECIALLY PATENT RIGHTS. IN PARTICULAR, master builders solutions DISCLAIMS ALL CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. master builders solutions SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. master builders solutions RESERVES THE RIGHT TO MAKE CHANGES ACCORDING TO TECHNoLOGY PROGRESS OR FUrTHER DEVELOPMENTS. IT IS THE CUSTOMERS RESPONSIBILITY AND OBLIGATION TO CAREFULLY INSPECT AND TEST ANY INCOMING GOODS. PERForMANCE OF THE PRODUCT(S) DESCRIBED HEREIN SHOULD BE VERIFIED BY TESTING AND CARRIED OUT ONLY BY QUALIFIED EXPERTS. IT IS THE SOLE RESPONSIBILITY OF THE CUSTOMER TO CARRY OUT AND ARRANGE FOR ANY SUCH TESTING. REFERENCE TO TRADE NAMES USED BY OTHER COMPANIES IS NEITHER A RECOMMENDATION, NOR AN ENDORSeMENT OF ANY PRODUCT AND DOES NOT IMPLY THAT SIMILAR PRODUCT COULD OR COULD NOT BE USED.