SECTION 09 67 23

MasterTop 1817 SRS PC Methyl-methacrylate Based Polymer Concrete

PART 1 GENERAL

1.01	WORK INCLUDED:

A.	Provisions established within the Contract, Division 1, General Requirements, the Drawings are collectively applicable to this Section.

B.	Related sections Section 09770 Special Protective Wall Coatings.

1.02	Products installed but not furnished under this section:

A.	Division 3 - Concrete (poured in place).

B.	Division 7 - Sealants: Control joints, expansion joints and doorframes.

C.	Division 15 - Mechanical: Drains

1.03	SYSTEM DESCRIPTION

A.	The overlay/patching mortar shall be a two-component system based on solvent-free, 100% reactive Methyl Methacrylate (MMA) Acrylic liquid and a powder component composed primarily of sand, polymers, and other inert fillers along with a curing agent.

B.	The polymer concrete cures to full mechanical strengths, full chemical resistances, and be available to normal traffic in no more than 90 minutes at 68°F.  The cured material has a minimum compressive strength of 7,800 psi in accordance with ASTM C39. Cured overlays have an abrasion resistance at least twice that of standard 3,000 psi concrete in accordance with ASTM C501.

C.	The finished floor coating/patching system shall be uniform in color, texture, and appearance.  All edges that terminate at walls, floor discontinuities, and other embedded items shall be sharp, uniform, and cosmetically acceptable with no thick or ragged edge.  The Contractor shall work out an acceptable masking technique to ensure the acceptable finish of all edges.

1.04	REFERENCE STANDARDS

A.	NACE No. 6/SSPC-SP 13 - Surface Preparation of Concrete

B.	ACI 308 – Standard Practice for Curing Concrete

C.	ACI 302.1R-80 - Guide for Concrete Floor and Slab Construction

D.	American Society for Testing and Materials (ASTM)

1.05	SUBMITTALS:

A.	Prior to commencing work, submit manufacturer’s technical information and installation details to describe materials to be used.  The same manufacturer shall supply all polymer underlayments wall and floor finishes.

B.	Submit manufacturer’s certificate of compliance that materials meet specification requirements.

C.	Before beginning work, samples of the flooring system shall be provided for architect’s approval.

1.06	QUALITY ASSURANCE:

A.	Manufacturer Qualifications:

1.	Master Builders Solutions  889 Valley Park Drive, Shakopee, MN 55375 Phone: 800-433-9517

2. No request for substitution shall be considered that would change the generic type of coating system specified (i.e., 100% reactive, Methyl Methacrylate based acrylic liquid).  Equivalent materials of other     manufacturer's may be substituted only on approval of the Architect or Engineer.  Requests shall include the respective manufacturer's technical literature for each product giving the name, generic type, descriptive information, recommended dry film thickness (DFT), Material Safety Data Sheet (MSDS), and certified test reports showing results to equal performance criteria of products specified herein.

3.	Manufacturer must show a minimum 10 year history of manufacturing MMA products for the specified application. Manufacturer must show a minimum of 10 projects of equal size and magnitude as this project.

B.	Applicator Qualifications:

1.	Pre-qualification requirements: Each bidder for this project shall be pre-qualified and approved by the material manufacturer at the time of bid submittal. Acceptability will include judgment on equipment, history, and financial strength.  In no case will Master Builders Solutions permit the application of any of its materials by untrained, non-approved Contractor or personnel.

2.	Each approved applicator shall have been trained by the Manufacturer in all phases of surface preparation and application of the specified flooring system(s).  Approved applicator must possess proper surface preparation equipment as recommended by manufacturer.

3.	Each approved applicator must have five years’ experience of installing the specified flooring system and submit a list of five projects/references as a prequalification requirement.  At least one of the five projects/references must be of equal size, quantity, and magnitude to this project as a prequalification requirement.  Owner has the option to personally inspect the projects/references to accept or reject any of the Contractors prior to bid time as a prequalification requirement.

C.	Acceptance Sample:

1.	A minimum one-foot square representative sample of the specified flooring system shall be prepared by the Manufacturer's representative and submitted to the Owner prior to the bidding phase of the project.  All bidders shall inspect the "acceptance sample" before submitting their bids.

2.	The installed flooring system shall be similar to the acceptance sample in thicknesses of respective film layers, color, texture, overall appearance and finish.

D.	Bond Testing:

1.	Surface preparation efforts shall be evaluated by conducting Bond Tests at the site prior to application of the flooring system(s).

2. 	See paragraph 3.03 or consult with Material Manufacturer for specific procedure.

E.	Pre-Job Meeting

1.	Owner requires a Pre-Job Meeting with representatives of Owner, Contractor/Applicator, and Material Manufacturer in attendance.  The agenda shall include a review and clarification of this specification, application procedures, quality control, inspection and acceptance criteria, and production schedules. Applicator is not authorized to proceed until this meeting is held or waived by Owner.

1.07	DELIVERY AND STORAGE:

A.	Material shall be delivered to project site in manufacturer’s original unopened containers bearing manufacturer’s name, product and color.

B.	Materials shall be stored indoors, protected from damage, moisture, direct sunlight and temperatures below 50 degrees F or above 80 degrees F.

1.08	PROJECT CONDITIONS

A.	Evaluate the substrate condition, including moisture content and extent of substrate leveling and repairs required, if any.

B.	Coordinate flooring work with other trades to ensure adequate illumination, ventilation, and dust free environment during application and curing of flooring.

- Comply with material manufacturer’s recommended temperature limitations for flooring application.

1.09	WARRANTY:

A.	Contractor shall furnish a written warranty covering both material and workmanship for a period of (      ) year from date of installation.

PART 2 PRODUCTS

2.01	MANUFACTURER:

Master Builders Solutions

889 Valley Park Drive

Shakopee, MN  55379 USA

Customer Service:  800-433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Website: www.master-builders-solutions.com/en-us

2.02	MATERIALS:

- MasterTop 1817 SRS PC Polymer Concrete :

- Saturating Primer/Sealer Coat:
MasterTop SRS 41P (formerly SRS R41 Degadur)

2. Patching/Sloping (if required)
MasterTop 1817 SRS PC Polymer Concrete

3. Topcoat (if required):
MasterTop SRS 71TC Colorless Topcoat Resin

    - Product Performance Criteria

A.	MasterTop SRS 41P Primer/Sealer

| 1. | Percentage Reactive Resin: | 100% |
| --- | --- | --- |
|  | Percentage Solids | 100% |
| 2. | Water Absorption, Wt. % (ASTM D570): | less than 0.6 |
| 3. | Tensile Strength, psi (ASTM D638) | 3550 |
| 4. | Tensile Modulus, psi X 10 to the 5th (ASTM D638): | 2.1 |
| 5. | Coefficient of Thermal Expansion, in./in./deg. F (ASTM D696): | .000035 |
| 6. | Electrical Resistivity (ASTM D257): |  |
|  | Volume Resistance, ohm-cm: | 1015 |
|  | Surface Resistance, ohm: | 1012 |
| 7. | Water Vapor Transmission (DIN 53122), g/cm-hr-mm Hg X 10-9: | 1.4 |

B. MasterTop 1817 SRS PC Polymer Concrete

| 1. | Percentage of reactive resin | 100% |
| --- | --- | --- |
| 2. | Water Absorption, Wt. % (ASTM D570): | 0.02 |
| 3. | Tensile Strength, psi (ASTM D638) | 1200 |
| 4. | Tensile Modulus, psi X 10 to the 5th (ASTM D638): | 1.2 |
| 5. | Coefficient of Thermal Expansion, in./in./deg. F (ASTM D696) psi x10-6: | 18 |
| 6. | Compressive Strength, psi (ASTM C39) | 7,000 |
|  | (ASTM C109) | 9,200 |

C. MasterTop SRS 71TC Colorless Topcoat Resin

| 1. | Percentage Reactive Resin: | 100% |
| --- | --- | --- |
|  | Percentage Solids: | 100% |
| 2. | Water Absorption, Wt. % (ASTM D570): | 0.04 |
| 3. | Tensile Strength, psi (ASTM D638): | 3555 |
| 4. | Tensile Modulus, psi (ASTM D638): | 210,000 |
| 5. | Coefficient of Thermal Expansion (ASTM D696) | .000035 in./in. Deg. F |
| 6. | Electrical Resistivity (ASTM D257): |  |
|  | Volume Resistance, ohm-cm: | 1015 |
|  | Surface Resistance, ohm: | 1012 |
| 7. | Water Vapor Transmission (DIN 53122) g/cm-hr-mm Hg X 10-9: | 1.43 |

8.	Chemical Resistance, ASTM D543:
Effect of weak acids:	none
Effect of strong acids:	slight
Effect of alkalis:	none
Effect of salt solutions:	none
Effect of oil, grease:	none
Effect of sunlight (UV radiation):	none

2.2.2	PRODUCT INSTALLATION & APPLICATION CRITERIA

A.	All MasterTop SRS Material Systems:

1.	Pot Life at 68° F.:			10-15 minutes

2.	Cure Time at 68° F.:		60 minutes

3.	Recoat Time at 68° F.:		60-90 minutes

# PART 3 EXECUTION

3.01	SURFACE CONDITIONS:

A.	Concrete must have a curing period of 28 days minimum at 70° F.  The surface must be clean and dry, physically sound and free of contamination.  Surfaces must be free of holes, voids or defects.  Cracks and abrupt changes in surface profile must be corrected.  Fins and projections must be removed.  All curing compounds and sealers must be removed.

B.	Verify that moisture content is within range acceptable to flooring manufacturer, using calcium chloride test kit in accordance with ASTM F-1869.

C.	Contractor must report, in writing, surfaces left in improper condition by other trades.  Application will constitute acceptance of surfaces by the applicator.

3.02	PREWORK INSPECTION

A.	Examine all surfaces to be coated with MMA material systems and report to the Owner and/or Engineer any conditions that will adversely affect the appearance or performance of these coating systems and that cannot be put into acceptable condition by the preparatory work specified in Paragraph 3.03.

B.	Do not proceed with application until the surface is acceptable or authorization to proceed is given by the Engineer.

C.	In the event that Applicator has employed all acceptable methods of surface preparation and cannot remedy adverse conditions that would lead to failure of the installation, Applicator shall withdraw from the contract and Owner will be financially responsible only for preparation efforts.

3.03	PREPARATION:

A.	Surface Preparation - General

1.	Concrete substrate must be clean and dry.  Dislodge dirt, mortar spatter, paint overspray, and other dry surface accumulations and contamination by scraping, brushing, sweeping, vacuuming, and/or compressed air blow-down.

2.	New concrete: See 1.08 - C for requirements.

3.	Surfaces that are heavily contaminated shall be cleaned with the appropriate degreaser, detergent, or other appropriate cleaner/surfactant followed by thoroughly rinsing with fresh water to remove the accumulation prior to mechanical cleaning efforts.  Mechanical cleaning will not remove such deposits, but only drive them deeper.

4.	Concrete shall have a moisture emission rate of no more than 5 lbs. per 1000 sq. ft. per 24   hour period as determined by proper Calcium Chloride Testing.

B.	Bond Testing

1.	The applicator shall evaluate all surface preparation by conducting bond tests at strategic locations.

2.	Mix six (6) ounces of the primer to be used in the application with #10-#12 mesh, dry quartz sand until an easily trowelable mixture is obtained.  Add 10% by volume MasterTop SRS 100HD and mix well.  Apply palm-sized patties 1/8" to 1/4" thick.

3.	After one (1) hour at (68° F.), patties must be cured tack-free and cooled to ambient temperature of concrete.  Remove patties with hammer and chisel and examine fracture/delamination plane.  Concrete with fractured aggregate must be attached to the entire underside of the patty.

4.	If only laitance or a small amount of concrete is attached or if interface between patty and substrate is tacky, further substrate preparation is required.

5.	If further surface preparation is required, bond tests shall be conducted again when this has been completed.

6.	If no amount or kind of surface preparation produces satisfactory bond tests, the applicator shall report that to the Owner, Engineer, and Manufacturer.

C.	Mechanical Surface Preparation and Cleaning

1.	The MasterTop SRS 71TC system requires a CSP 4-5 in accordance with ICRI CSP Surface Preparation Standards.  All accessible concrete floor surfaces shall be mechanically blast cleaned using a mobile steelshot, dust recycling machine such as BLASTRAC, as manufactured by Wheelabrator Corp., or approved equivalent.  All surface and embedded accumulations of paint, toppings, hardened concrete layers, laitance, power trowel finishes, and other similar surface characteristics shall be completely removed leaving a bare concrete surface having a profile similar to 40 grit sandpaper and exposing the upper fascia of concrete aggregate.

2.	Floor areas inaccessible to the mobile blast cleaning machines shall be mechanically abraded to the same degree of cleanliness, soundness, and profile using vertical disc scarifiers, starwheel scarifiers, needle guns, scabblers, or other suitably effective equipment.

3.	After blasting, traces or accumulations of spent abrasive, laitance, removed toppings, and other debris shall be removed with brush or vacuum.

4.	Conduct Bond Tests to check adequacy of surface preparation.  See Paragraph 3.03 - B (Bond Testing).

5.	Application of the respective specified material system(s) must be completed before any water or other contamination of the surface occurs.

3.04	INSTALLATION:

# A. Application of MasterTop 1817 SRS PC Polymer Concrete consists of:

# 1) Applying the primer, MasterTop SRS 41P.

# 2) Applying the MasterTop 1817 SRS PC system.

# B. Time for curing (60-90 minutes) shall be allowed between each coat.

# C. Thicknesses are specified below and/or in Paragraph 3.07.

D.  Open only the containers of component materials to be used in each specific application as needed.  Refer to Manufacturer's data sheets for pot-life/temperature relationship to determine size of batches to mix and mix ratios for each respective coat of the system.

# E.   Pot life is short, so mix only as much material at a time as can be easily and efficiently applied.

3.04.1 PRIME COAT

A.	Measure, add, and mix the MasterTop SRS 103IN, and initiator (MasterTop SRS 100HD) into the respective resin components in the proportions recommended by the Material Manufacturer.

B.	Pour the mixture batches onto the floor surface and use a 9" or 18" wide, 1/2" - 3/4" thick-napped, solvent-resistant paint roller to roll out the material at a rate of 100 sq. ft./ gal. to form a uniform, continuous film, ensuring that all crevices, cracks, other surface discontinuities have been saturated and coated.  Use a paint brush to reach areas inaccessible to the roller. Work quickly and deliberately; the pot life is short (10 -15 minutes).  Do not leave any "puddles"; roll out any such accumulations.

C.	Allow the primer/sealer coat to cure.

D.	If any of the concrete has absorbed all of the primer or if the concrete still has a dry look, re-prime these areas before applying bodycoat or topcoat.

3.04.3 PATCHING/SLOPING

- Measure, add, and mix the MasterTop 1817 SRS PC Resin, Powder Component, and necessary aggregate (if required) in the proportions recommended by the Material Manufacturer.

- Use mixture to repair any damaged concrete, or to slope any areas as needed.

- Once cured, material must be re-primed before topping system is applied.

3.04.4 TOP COAT (if required)

A.	Apply with clean rollers at a rate of 90 - 100 sq. ft./gal. in the same way as the Primer/Sealer was applied as described in Paragraph 3.04.01.

B.	Allow topcoat to cure.

3.05  FIELD QUALITY CONTROL/INSPECTION

A.	Applicator shall request acceptance of surface preparation from the Engineer before application of the prime/seal coat.

B.	Applicator shall request acceptance of the prime/seal coat from the Engineer before application of subsequent specified materials.

C.	All work not acceptable to the Architect, Engineer, or Owner must be corrected before consideration of final acceptance.

3.06  CLEANING

A.	Applicator shall remove any material spatters and other material that is not where it should be.  Remove masking and covers taking care not to contaminate surrounding area.

B.	Applicator shall repair any damage that should arise from either the application or clean-up effort.

3.07  COATING SCHEDULE

- Primer shall be MasterTop SRS 41P. Application rate shall be approx.100 sq.ft. per gallon (approx. 12 mils).

- Patching/Sloping material shall be MasterTop 1817 SRS PC.

- Clear topcoat shall be MasterTop SRS 71TC; apply at the rate of 90 - 100 sq. ft. per gallon for the first coat and 100 - 125 sq. ft. per gallon for the second application.

3.07  MANUFACTURERS RECOMMENDATIONS

- For more specific information concerning maintaining Methyl Methacrylate floors please consult the manufacturer at the above location.

END OF SECTION

Disclaimer

THIS INFORMATION AND ALL FURTHER TECHNICAL ADVICE ARE BASED ON master builders solutions PRESENT KNOWLEDGE AND EXPERIENCE. HOWEVER, master builders solutions ASSUMES NO LIABILITY FOR PROVIDING SUCH INFORMATION AND ADVICE INCLUDING THE EXTENT TO WHICH SUCH INFORMATION AND ADVICE MAY RELATE TO EXISTING THIRD-PARTY INTELLECTUAL PROPERTY RIGHTS, ESPECIALLY PATENT RIGHTS. IN PARTICULAR, master builders solutions DISCLAIMS ALL CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. master builders solutions SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. master builders solutions RESERVES THE RIGHT TO MAKE CHANGES ACCORDING TO TECHNoLOGY PROGRESS OR FUrTHER DEVELOPMENTS. IT IS THE CUSTOMERS RESPONSIBILITY AND OBLIGATION TO CAREFULLY INSPECT AND TEST ANY INCOMING GOODS. PERForMANCE OF THE PRODUCT(S) DESCRIBED HEREIN SHOULD BE VERIFIED BY TESTING AND CARRIED OUT ONLY BY QUALIFIED EXPERTS. IT IS THE SOLE RESPONSIBILITY OF THE CUSTOMER TO CARRY OUT AND ARRANGE FOR ANY SUCH TESTING. REFERENCE TO TRADE NAMES USED BY OTHER COMPANIES IS NEITHER A RECOMMENDATION, NOR AN ENDORSeMENT OF ANY PRODUCT AND DOES NOT IMPLY THAT SIMILAR PRODUCT COULD OR COULD NOT BE USED.