SECTION 03 62 13

MasterFlow® 100 Grout

Notes to specifiers:

Please update your Master Specifications to reflect the company and product name changes. The old product names are provided in parentheses following the new names in this Section for reference.

The purpose of this guide specification is to assist the specifier in developing a project specification for the use of master buidlers solutions products.  this guide document has been prepared to be part of a complete project manual.  it is not intended to be a “stand alone” document, and it is not intended to be copied directly into a project manual.

This guide specification will need to be carefully reviewed for APPROPRIATENESS for the given project and edited accordingly to comply with project-specific requirements.

GENERAL

SUMMARY

Section Includes:

Application of noncatalyzed, mineral-aggregate, non-shrink grout.

Delete sections below not relevant to this project; add others as required.

Related Sections:

          - Section 03 30 00 – Cast-in-Place Concrete.

          - Section 03 45 00 – Precast Architectural Concrete.

          - Section 05 12 00 – Structural Steel Framing.

          - Section 05 50 00 – Metal Fabrications.

          - Section 31 40 00 – Shoring and Underpinning.

SUBMITTALS

Comply with Section [01 33 00] [ __ __ __ ].

Product Data:  Submit manufacturer's technical data sheets,

LEED Submittals:  Comply with requirements for each product to achieve points indicated in LEED Project Checklist provided by the architect/engineer.

Submit list of project references as documented in this specification under Quality Assurance Article.  Include contact name and phone number of the person charged with oversight of each project.

Quality Control Submittals:

Provide protection plan of surrounding areas and non-cementitious surfaces.

QUALITY ASSURANCE

Comply with Section [01 40 00] [ __ __ __ ].

Qualifications:

          - Manufacturer Qualifications:  Company with minimum 15 years of experience in manufacturing of specified products.

          - Manufacturer Qualifications: Company shall be ISO 9001:2015 Certified.

          - Applicator Qualifications:  Company with minimum of 5 years’ experience in application of similar products on projects of similar size and scope and is acceptable to product manufacturer.

Successful completion of a minimum of 3 projects of similar size and complexity to specified work.

Delete below if work of this Section is not extensive or complex enough to justify a pre-installation conference.  If retaining, coordinate with Division 1.

Pre-Installation Meetings:  Conduct meeting at project site to comply with requirements in Section 01 31 00 – Project Management and Coordination.

Schedule and convene meeting a minimum of one week before starting work of this section.

Review weather conditions, surface preparation, mixing, application, curing and protection.

Discuss procedures for protecting adjacent finished work.

Provide manufacturer’s representative with 10 days written notice of pre-installation meeting.

DELIVERY, STORAGE, AND HANDLING

Comply with Section [01 60 00] [ __ __ __ ].

Comply with manufacturer’s ordering instructions and lead-time requirements to avoid construction delays.

Deliver materials in manufacturer's original, unopened, undamaged containers with identification labels intact.

Store materials in unopened packaging in clean, dry area protected from sunlight.  Prevent material from freezing.

PROJECT CONDITIONS

Environmental Requirements:

Place grout between 50 and 90 degrees F (10 and 32 degrees C).

PRODUCTS

MANUFACTURERs

Subject to compliance with requirements, provide products from the following manufacturer:

Master Builders Solutions

889 Valley Park Drive

Shakopee, MN  55379 USA

Customer Service:  800-433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Website: www.master-builders-solutions.com/en-us

Substitutions:  Comply with Section [01 60 00] [ __ __ __ ].

Specifications and Drawings are based on manufacturer's proprietary literature from Master Builders Solutions.  Other manufacturers shall comply with minimum levels of material and detailing indicated in Specifications or on Drawings.  Architect/Engineer will be sole judge of appropriateness of substitutions.

MATERIALS

Noncatalyzed, mineral-aggregate, non-shrink grout.

Acceptable Product:  MasterFlow 100 (formerly Construction Grout) by Master Builders Solutions.

Performance Requirements:  Provide grout complying with the following requirements:

          - Compliances:

ASTM C1107, Grade C, at flowable or plastic consistency.

Corps of Engineers CRD C621, Grade C, at flowable or plastic consistency.

          - Flow, ASTM C230, 5 drops:  126 to 145 percent.

          - Volume Change, Flowable Consistency, ASTM C1090, after 28 days:  0.01 percent.

          - Compressive Strength, Flowable Consistency, ASTM C942 according to ASTM C1107:

1 Day:  2,000 psi (13.8 MPa).

3 Days:  5,000 psi (34.5 MPa).

7 Days:  6,000 psi (41.3 MPa).

28 Days:  7,000 psi (48.0 MPa).

          - Color:  Concrete gray when cured.

          - VOC Content:  0 lbs per gal (0 g/L), less water and exempt solvents.

EXECUTION

EXAMINATION

Comply with Section [01 70 00] [ __ __ __ ].

SURFACE Preparation

Prepare surfaces in accordance with manufacturer’s instructions.

Clean steel surfaces of dirt, oil, grease, and other contaminants.

Ensure surface to be grouted is clean, sound, and roughened to CSP of 5 to 9 in accordance with ICRI Guideline 03732 to permit proper bond.

Saturate concrete surfaces with clean water for 24 hours immediately before grouting.

Remove freestanding water immediately before grouting.

Shade foundation from sunlight 24 hours before and 24 hours after grouting.

delete the following article if no metal base plates on project.

Allow minimum of 1 inch (25 mm) vertical clearance under baseplates.

mixing

Mix materials in accordance with manufacturer’s instructions.

Use minimum amount of water to provide desired workability.

Mix materials until uniform consistency is attained.

Do not use water in amount or temperature to cause bleeding or segregation.

application

Place grout in accordance with manufacturer’s instructions.

Do not place grout in lifts greater than 6 inches (152 mm) unless grout is extended with aggregate to dissipate hydration heat.

Curing

Cure grout in accordance with manufacturer’s instructions.

Cure exposed grout shoulders by wet curing for 24 hours.

Apply membrane curing compound approved by grout manufacturer and compliant with ASTM C309 or preferably ASTM C1315.

PROTECTION

Protect completed grout from damage during construction.

END OF SECTION

Disclaimer.

THIS INFORMATION AND ALL FURTHER TECHNICAL ADVICE ARE BASED ON master builders solutions PRESENT KNOWLEDGE AND EXPERIENCE. HOWEVER, master builders solutions ASSUMES NO LIABILITY FOR PROVIDING SUCH INFORMATION AND ADVICE INCLUDING THE EXTENT TO WHICH SUCH INFORMATION AND ADVICE MAY RELATE TO EXISTING THIRD-PARTY INTELLECTUAL PROPERTY RIGHTS, ESPECIALLY PATENT RIGHTS. IN PARTICULAR, master builders solutions DISCLAIMS ALL CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. master builders solutions SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. master builders solutions RESERVES THE RIGHT TO MAKE CHANGES ACCORDING TO TECHNoLOGY PROGRESS OR FUrTHER DEVELOPMENTS. IT IS THE CUSTOMERS RESPONSIBILITY AND OBLIGATION TO CAREFULLY INSPECT AND TEST ANY INCOMING GOODS. PERForMANCE OF THE PRODUCT(S) DESCRIBED HEREIN SHOULD BE VERIFIED BY TESTING AND CARRIED OUT ONLY BY QUALIFIED EXPERTS. IT IS THE SOLE RESPONSIBILITY OF THE CUSTOMER TO CARRY OUT AND ARRANGE FOR ANY SUCH TESTING. REFERENCE TO TRADE NAMES USED BY OTHER COMPANIES IS NEITHER A RECOMMENDATION, NOR AN ENDORSeMENT OF ANY PRODUCT AND DOES NOT IMPLY THAT SIMILAR PRODUCT COULD OR COULD NOT BE USED.