SECTION 07 92 19

MasterSeal® NP 520 Sealant

Notes to specifiers:

Please update your Master Specifications to reflect the company and product name changes. The old product names are provided in parentheses following the new names in this Section for reference.

The purpose of this guide specification is to assist the specifier in developing a project specification for the use of master buidlers solutions products.  this guide document has been prepared to be part of a complete project manual.  it is not intended to be a “stand alone” document, and it is not intended to be copied directly into a project manual.

This guide specification will need to be carefully reviewed for APPROPRIATENESS for the given project and edited accordingly to comply with project-specific requirements.

GENERAL

system description

Section Includes:

Application of acoustical joint sealant.

Related Sections:

edit note:  if retaining related sections article, delete sections from this list or add sections per project requirements.

Section 03 30 00 – Cast-in-Place Concrete.

Section 04 21 00 – Masonry Assemblies Unit Masonry.

Section 08 41 00 – Aluminum Entrances and Storefronts.

Section 08 81 00 – Glass Glazing.

SUBMITTALS

Comply with Section [01 33 00] [__ __ __].

Product Data:  Submit manufacturer's technical data sheets.

LEED Submittals:  Comply with requirements for each product to achieve points indicated in LEED Project Checklist provided by the architect/engineer.

Samples:

Initial Selection Purposes:  For each product exposed to view, manufacturer's standard bead consisting of strips of actual products showing full range of colors available.

Verification:  Two sets of each type and color of joint sealant required.  Install joint sealant samples in 1/2-inch wide joints formed between two 6-inch long strips of material matching appearance of exposed surfaces adjacent to joint sealants.

Submit laboratory tests or data validating product compliance with performance criteria specified.

Submit list of references from 5 projects similar in scope to this Project.  Include contact name and phone number of the person charged with oversight of each project.

Warranty:  Provide manufacturer's standard material warranty.

QUALITY ASSURANCE

Comply with Section [01 40 00] [__ __ __].

Qualifications:

Manufacturer Qualifications:  Company regularly engaged in manufacturing and marketing of products specified in this Section.

Manufacturer Qualifications:  Company shall be ISO 9001:2015 Certified.

Applicator Qualifications:  Qualified to perform work specified by reason of experience or training provided by product manufacturer.

Mock-Ups:

At start of project, perform mock-up of required sealant work at one area of building.  Perform minimum of one mock-up for each different combination of substrates to be sealed.  Coordinate mock-up areas with architect/engineer.

Install mock-ups and test in presence of sealant manufacturer’s authorized representative and architect/engineer to ensure application procedures are consistent with warranty requirements.

After sealant has achieved sufficient cure as coordinated with manufacturer’s representative, conduct adhesion pull-tests or non-destructive testing, at discretion of architect/engineer.  Conduct tests in accordance with ASTM C1521.

Confirm results of adhesion tests as acceptable to Architect and sealant manufacturer before starting work.

Leave approved mock-ups in place to establish standards and guidelines for acceptable application of sealant Work and acceptable appearance.

DELIVERY, STORAGE, AND HANDLING

Comply with Section [01 60 00] [__ __ __].

Deliver products in original factory packaging bearing identification of product, manufacturer, and batch number.

Store products in original, unopened containers in clean, dry area away from heat and direct sunlight.  Do not store below 40°F.

PROJECT CONDITIONS

Do not use products under conditions of precipitation or in inclement or freezing weather.  Verify that substrates are clean, dry, and frost free.  Use appropriate measures for protection and supplementary heating to ensure proper curing conditions in accordance with manufacturer's recommendations if application during inclement weather occurs.

PRODUCTS

MANUFACTURERs

Subject to compliance with requirements, provide products from the following manufacturer:

Master Builders Solutions

889 Valley Park Drive

Shakopee, MN  55379 USA

Customer Service:  800-433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Website: www.master-builders-solutions.com/en-us

Substitutions:  Comply with Section [01 60 00] [__ __ __].

Specifications and drawings are based on manufacturer's proprietary literature from BASF.  Other manufacturers shall comply with minimum levels of material, color selection, and detailing indicated in specifications or on drawings.  Architect/engineer will be sole judge of appropriateness of substitutions.

MATERIALS

        - A one component, non-priming, siliconized acrylic latex sealant that is fire-rated and designed to be used as an acoustical sealant in partition systems.

Acceptable Product:  MasterSeal NP 520 Sealant

Performance Requirements:  Provide sealant complying with the following requirements:

Compliances:

Exceeds the standard specification for latex sealants ASTM C834, Type OP, Grade -18 degrees C.

STC (Sound Transmission Class) Level of 58 as tested by ASTM E90.

Meets Class A for smoke development and flammability test by ASTM E84 or UL 723

Adhesion Loss, ASTM C736:  0.5 percent.

Artificial Weathering, ASTM C732:  No adhesion loss, cracking, discoloration, slump, or wash-out.

Elongation at Break, ASTM D412:  169 percent.

Extrusion Rate, ASTM C731:  9.8 g/sec.

100% Modulus, ASTM D412:  199 psi.

Recovery, ASTM C736:  91.3 percent.

Slump, ASTM D2202:  0 in.

Stain Index, ASTM D2203: 1.1.

Tack Free Time, ASTM D2377 (Pass/Fail):  Pass.

Tensile Strength, ASTM D412:  203 psi.

Volume Shrinkage, ASTM C7:  25-28 percent.

Sound Transmission Class, ASTM E90:  58 dB.

Flame Spread Index, ASTM 84 or UL723:  10.

Smoke Development Index, ASTM 84 or UL723:  5.

VOC Content:  13 g/L, less water and exempt solvents.

Design Requirements:

Design number of joints and joint widths for maximum of plus or minus 50 percent movement.

Design depth of sealant to be 1/2 width of joint.

Maximum Depth:  1/2 inch (13 mm).

Minimum Depth:  1/4 inch (6 mm).

Maximum Recommended Width: 1-1/2 inches (38 mm).

COLOR

Sealant Colors:  Selected by Architect from manufacturer’s full color range.

NP 520 colors:

White

Ash Brown

Aluminum Stone

Brown

Cameo

Summer Gray

Almond

Dark Tan

Coppertone

Black

Bronze

EXECUTION

EXAMINATION

Comply with Section [01 70 00] [__ __ __].

Inspect areas involved in work to establish extent of work, access and need for protection of surrounding construction.

Examine joints for defects that would adversely affect quality of installation.

Provide additional joint preparation, beyond that outlined in Specifications, as required by sealant manufacturer and Architect’s recommendations based on mock-ups and field adhesion tests.

Install sealants between 40°F and 110°F, substrate surface temperature

SURFACE PREPARATION

Prepare surfaces in accordance with manufacturer’s instructions.

Clean joints as required to expose sound surface free of contamination and laitance.

Ensure structurally sound surfaces, dry, clean, free of dirt, moisture, loose materials, oil, grease, asphalt, tar, paint, wax, rust, waterproofing, curing and parting compounds, membrane materials, and other foreign matter that impair adhesion of sealant.

Concrete, Stone, and Other Masonry:

Clean by grinding, sandblasting, or wire brushing to expose sound surface free of contamination and laitance.

Wood:

Clean new and weathered wood.  Scrape away loose paint to bare wood.  If coatings cannot be removed, test coatings to verify adhesion of sealant or determine appropriate primer.

Metal:

Remove scale, rust, and coatings from metal to expose bright white surface.  Remove protective coatings and chemical residue or film.

Aluminum Frames:  Remove clear lacquer before application of joint sealants.  If coatings cannot be removed, test coatings to verify adhesion of sealant or determine appropriate primer.

Remove other protective coatings or finishes that could interfere with adhesion.

Priming

Where circumstances or substrates require primer, comply with the following requirements:

Apply primer in accordance with manufacturer’s instructions.

Allow primer to dry before applying joint sealants.

Prime and seal on same workday.

APPLICATION

Back-Up Material:

Install appropriate size backer rod, larger than joint where necessary in accordance with manufacturer's recommendations, and in manner to provide concave sealant profile.

Where joint depth does not permit installation of backer rod, install adhesive-backed polyethylene bond-breaker tape along entire back of joint to prevent 3-sided adhesion of joint sealant.

Sealant:

Apply sealant in accordance with manufacturer’s instructions.

Verify that temperature and moisture conditions are within manufacturer’s acceptable limits.

Completely fill joint with sealant, filling from bottom up to avoid entrapping air.

Using clean, dry tool with rounded edge, and of appropriate width for each joint, tool freshly installed sealant to provide preferred concave profile, to ensure intimate contact between sealant and substrate, and to provide neat appearance.  Where surface aggregate does not permit proper tooling, install sealant and backer rod so that face of joint is recessed behind exposed aggregate, and sealant is bonded to firm, even surface.

Use dry tooling method.  Do not use tooling agents such as soapy water or solvents that have not been approved by sealant manufacturer.

Curing

Allow sealant to cure in accordance with manufacturer’s instructions.

INSPECTION

During work of the section, inspect work to ensure compliance with manufacturer’s instructions, specifications, and drawings.

Evaluate adhesion of sealant in accordance with ASTM C1521.

Allow inspections of work and assist in testing requested by manufacturer’s representative and architect/engineer.

Non-Compliant Work:  If inspections reveal non-compliant work or work that was not installed in accordance with Specifications, and/or manufacturer requirements, remove adjacent Work until a location is reached where installation was performed properly.  Assist in spot-checking of remainder of Work.

CLEANING

Remove excess sealant in accordance with manufacturer’s instructions.

PROTECTION

Protect sealant from damage during construction.

END OF SECTION

Disclaimer:

THIS INFORMATION AND ALL FURTHER TECHNICAL ADVICE ARE BASED ON master builders solutions PRESENT KNOWLEDGE AND EXPERIENCE. HOWEVER, master builders solutions ASSUMES NO LIABILITY FOR PROVIDING SUCH INFORMATION AND ADVICE INCLUDING THE EXTENT TO WHICH SUCH INFORMATION AND ADVICE MAY RELATE TO EXISTING THIRD-PARTY INTELLECTUAL PROPERTY RIGHTS, ESPECIALLY PATENT RIGHTS. IN PARTICULAR, master builders solutions DISCLAIMS ALL CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. master builders solutions SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. master builders solutions RESERVES THE RIGHT TO MAKE CHANGES ACCORDING TO TECHNoLOGY PROGRESS OR FUrTHER DEVELOPMENTS. IT IS THE CUSTOMERS RESPONSIBILITY AND OBLIGATION TO CAREFULLY INSPECT AND TEST ANY INCOMING GOODS. PERForMANCE OF THE PRODUCT(S) DESCRIBED HEREIN SHOULD BE VERIFIED BY TESTING AND CARRIED OUT ONLY BY QUALIFIED EXPERTS. IT IS THE SOLE RESPONSIBILITY OF THE CUSTOMER TO CARRY OUT AND ARRANGE FOR ANY SUCH TESTING. REFERENCE TO TRADE NAMES USED BY OTHER COMPANIES IS NEITHER A RECOMMENDATION, NOR AN ENDORSeMENT OF ANY PRODUCT AND DOES NOT IMPLY THAT SIMILAR PRODUCT COULD OR COULD NOT BE USED.