Section 09 67 23

MasterTop 1245 CLAD Epoxy Flooring System

PART 1 GENERAL

1.01   WORK INCLUDED

- Special epoxy flooring system materials, including underlayments, waterproofing membranes, primers, fillers, and other applied materials used as underlayments, prime, body coat and finish coats, and the application of these materials.

- Related sections Section 09770 Special Protective Wall Coatings.

1.02	Products installed but not furnished under this section:

- Division 3 - Concrete (poured in place).

- Division 7 - Sealants: Control joints, expansion joints and doorframes.

- Division 15 - Mechanical: Drains

1.03	REFERENCE STANDARDS

- NACE No. 6/SSPC-SP 13 - Surface Preparation of Concrete

- ACI 308 – Standard Practice for Curing Concrete

- ACI 302.1R-80 - Guide for Concrete Floor and Slab Construction

- American Society for Testing and Materials (ASTM)

- Military Specification (MIL)

MIL-D-3134 Deck Covering Material

MIL-D-24613 Deck Covering Materials, Interior Cosmetic Polymeric

1.04	SUBMITTALS

- Prior to commencing work, submit manufacturer’s technical information and installation details to describe materials to be used.  The same manufacturer shall supply all polymer underlayments, wall and floor finishes.

- Owner and Contractor shall review and mutually agree upon color, grade and final texture of special epoxy floor system before starting installation.

- Before beginning work, samples of the polymer flooring shall be provided for the architect’s approval.

1.05	QUALITY ASSURANCE

- Contractor shall be an established firm regularly engaged in satisfactory installation of similar materials and shall provide a list of 3 projects of similar nature and complexity completed in the last 5 years.  Contractor shall provide a letter of certification by manufacturer that Contractor is a current qualified installer.

- Single source responsibility: Provide fillers, broadcast media, underlayments, epoxy primer, body coat and Topcoat coat produced by the same manufacturer with no less than 10 years of experience in the manufacture and supply of these principal materials for work in this section.

- Prior to commencing the installation, the Contractor shall install, with Owner’s approval, a mutually agreed upon sample (“mock-up”) to show final color and texture of the system.  This mock-up shall serve as a job standard for the final installation.

1.06	DELIVERY AND STORAGE:

- Material shall be delivered to project site in manufacturer’s original unopened containers bearing manufacturer’s name, product and color.

- Materials shall be stored indoors, protected from damage, moisture, direct sunlight and temperatures below 50 degrees F or above 80 degrees F.

1.07	PROJECT CONDITIONS

- Evaluate the substrate condition, including moisture content and extent of substrate leveling and repairs required, if any.

- Coordinate flooring work with other trades to ensure adequate illumination, ventilation, and dust free environment during application and curing of flooring.

- Comply with material manufacturer’s recommended temperature limitations for flooring application.

1.08	WARRANTY:

- Contractor shall furnish a written warranty covering both material and workmanship for a period of (    ) year from date of installation.

PART 2 PRODUCTS

2.01	MANUFACTURER:

Master Builders Solutions

889 Valley Park Drive

Shakopee, MN  55379 USA

Customer Service:  800-433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Website: www.master-builders-solutions.com/en-us

2.02	MATERIALS

MASTERTOP 1245 CLAD SYSTEM, SELF LEVELING EPOXY FLOOR SYSTEM

- Seamless Polymer Flooring shall be a three-component epoxy floor system consisting of epoxy resin, cure agent and special graded aggregate applied to a minimum finished thickness of 1/4 inch.  Three-component special epoxy flooring system shall be trowel applied to 1/4 inch thickness in one application and finished with a minimum of two coats pigmented epoxy, polyurethane, or polyaspartic to achieve color and texture selected.

- System Consists of the following:

- Primer: MasterTop GP 500 Part A / Part B

250 sq.ft./gal.

- Basecoat:	MasterTop GP 500 Part A / Part B + MasterTop PGM 500 pigment pack + MasterTop F 500TG aggregate

50 sq.ft./batch

- Grout Coat:	MasterTop TC 504 Part A / Part B

100-120 sq.ft./gal.

- Finish Coat:	MasterTop TC 504 Part A / Part B

250 sq.ft./gal.

- Optional Finish Coat:

MasterTop TC 493 Polyurethane Top Coat

MasterTop TC 683 Polyaspartic Top Coat

- Physical Properties.  Epoxy Flooring Systems shall comply with the following minimum test standards:

| Compressive Strength, ASTM C 579 | 12,900 psi |
| --- | --- |
| Tensile Strength, ASTM D 638 | 8,000 psi |
| Flexural Strength, ASTM D 790 | 4,990 psi |
| Impact Resistance, MIL-D-3134 | No signs of chipping, cracking, or detachment |
| Abrasion Resistance, CS17 Wheel 1000 gram load, 1000 cycles ASTM D-4060 | .070 gram loss |
| Adhesive Strength, ASTM D-4541 | 350 psi |
| Rate of Burning, ASTM D635 | Self-Extinguishing |
| Oil Resistance, MIL-D-3135 | 0.20 |
| Shock Resistance, MIL-D-3135 | No signs of chipping, cracking, or detachment |
| Hardness Shore D ASTM D-2240 | 75 - 85 |

- Where chemical resistance is a requirement, add the following, followed by the chemicals and concentrations required:

“Special flooring shall show no chemical attack when tested in accordance with ASTM D 1308 for 7 days against the following reagents and concentrations noted.”

PART 3  EXECUTION

3.01	SURFACE CONDITIONS:

- Concrete must have a curing period of 28 days minimum at 70° F.  The surface must be clean and dry, physically sound and free of contamination.  Surfaces must be free of holes, voids or defects.  Cracks and abrupt changes in surface profile must be corrected.  Fins and projections must be removed.  All curing compounds and sealers must be removed.

- Verify that moisture content is within range acceptable to flooring manufacturer, using a calcium chloride test kit in accordance with test method ASTM F 1869.

- Contractor must report, in writing, surfaces left in improper condition by other trades.  Application will constitute acceptance of surfaces by the applicator.

3.02	PREWORK INSPECTION

- Examine all surfaces to be coated with Selby material systems and report to the Owner and/or Engineer any conditions that will adversely affect the appearance or performance of these coating systems and that cannot be put into acceptable condition by the preparatory work specified in Paragraph 3.03.

- Do not proceed with application until the surface is acceptable or authorization to proceed is given by the Engineer.

- In the event that Applicator has employed all acceptable methods of surface preparation and cannot remedy adverse conditions that would lead to failure of the installation, Applicator shall withdraw from the contract and Owner will be financially responsible only for preparation efforts.

3.03	PREPARATION:

A.   Surface Preparation - General

1.	Concrete substrate must be clean and dry.  Dislodge dirt, mortar spatter, paint overspray, and other dry surface accumulations and contamination by scraping, brushing, sweeping, vacuuming, and/or compressed air blow-down.

2.	 New concrete: See 1.08 - C for requirements.

3.  Surfaces that are heavily contaminated shall be cleaned with the appropriate degreaser, detergent, or other appropriate cleaner/surfactant followed by thoroughly rinsing with fresh water to remove the accumulation prior to mechanical cleaning efforts.  Mechanical cleaning without degreasing can drive these deposits further into the substrate.

4.	Concrete shall have a moisture emission rate of no more than 4 lbs. per 1000 sq. ft. per 24 hour period as determined by proper Calcium Chloride Testing.

B.	Mechanical Surface Preparation and Cleaning

1.	The MasterTop 1245 CLAD system requires a CSP 3-5 in accordance with ICRI CSP Surface Preparation Standards.  All accessible concrete floor surfaces shall be mechanically blast cleaned using a mobile steelshot, dust recycling machine such as BLASTRAC, as manufactured by Wheelabrator Corp., or approved equivalent.  All surface and embedded accumulations of paint, toppings, hardened concrete layers, laitance, power trowel finishes, and other similar surface characteristics shall be completely removed leaving a bare concrete surface having a profile similar to 40 grit sandpaper and exposing the upper fascia of concrete aggregate.

2.	Floor areas inaccessible to the mobile blast cleaning machines shall be mechanically abraded to the same degree of cleanliness, soundness, and profile using vertical disc scarifiers, starwheel scarifiers, needle guns, scabblers, or other suitably effective equipment.

3.	After blasting, traces or accumulations of spent abrasive, laitance, removed toppings, and other debris shall be removed with brush or vacuum.

4.	Application of the respective specified material system(s) must be completed before any water or other contamination of the surface occurs.

3.03	INSTALLATION

Comply with flooring system manufacturer’s recommendation.  Materials shall be prepared and mixed in compliance with flooring manufacturer’s instructions.  Apply primer as recommended by flooring manufacturer to completely seal substrate.  Using a trowel, install body coat at a nominal ¼” thickness or to the specified depth.

  - CLEAN UP

Remove waste materials, rubbish and debris and dispose of them in accordance with local regulations.  Leave work areas in a clean condition.

3.05	PROTECTION

- Protect the completed work from water, airborne particles or other surface contaminants until cured, tack free, approximately 18-24 hours after application.

- Protect completed system from traffic and physical abuse for approximately 72 hours.  Protect completed system from immersion and chemical exposure until thoroughly cured, approximately seven (7) days.

END OF SECTION

DISCLAIMER: THIS INFORMATION AND ALL FURTHER TECHNICAL ADVICE ARE BASED ON master builders solutions PRESENT KNOWLEDGE AND EXPERIENCE. HOWEVER, master builders solutions ASSUMES NO LIABILITY FOR PROVIDING SUCH INFORMATION AND ADVICE INCLUDING THE EXTENT TO WHICH SUCH INFORMATION AND ADVICE MAY RELATE TO EXISTING THIRD-PARTY INTELLECTUAL PROPERTY RIGHTS, ESPECIALLY PATENT RIGHTS. IN PARTICULAR, master builders solutions DISCLAIMS ALL CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. master builders solutions SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. master builders solutions RESERVES THE RIGHT TO MAKE CHANGES ACCORDING TO TECHNoLOGY PROGRESS OR FUrTHER DEVELOPMENTS. IT IS THE CUSTOMERS RESPONSIBILITY AND OBLIGATION TO CAREFULLY INSPECT AND TEST ANY INCOMING GOODS. PERForMANCE OF THE PRODUCT(S) DESCRIBED HEREIN SHOULD BE VERIFIED BY TESTING AND CARRIED OUT ONLY BY QUALIFIED EXPERTS. IT IS THE SOLE RESPONSIBILITY OF THE CUSTOMER TO CARRY OUT AND ARRANGE FOR ANY SUCH TESTING. REFERENCE TO TRADE NAMES USED BY OTHER COMPANIES IS NEITHER A RECOMMENDATION, NOR AN ENDORSeMENT OF ANY PRODUCT AND DOES NOT IMPLY THAT SIMILAR PRODUCT COULD OR COULD NOT BE USED.