Section 09 67 26

MasterTop 1254 (formerly Selbatwede HD) Epoxy Flooring System

PART 1 GENERAL

1.01	WORK INCLUDED

A.	Section Includes

- Special epoxy flooring system materials, including underlayments, waterproofing membranes, primers, fillers, and other applied materials used as underlayments,  prime, body coat and finish coats, and the application of these materials.

B.	Related Section

1.	Section 09770 Special Protective Wall Coatings

C.	Provisions established within the Contract, Division 1, General Requirements, the drawings are collectively applicable to this Section.

1.02	REFERENCE STANDARDS

A.	American Society for Testing and Materials (ASTM)

B.	Military Specification (MIL)

MIL-D-3134 Deck Covering Material

MIL-D-24613 Deck Covering Materials, Interior Cosmetic Polymeric

1.03	SUBMITTALS

A.	Prior to commencing work, submit manufacturer’s technical information and installation details to describe materials to be used.  The same manufacturer shall supply all polymer underlayments, wall and floor finishes.

B.	Owner and Contractor shall review and mutually agree upon color, grade and final texture of special epoxy floor system before starting installation.

C.	Before beginning work, samples of the polymer flooring shall be provided for the architect’s approval.

1.04	QUALITY ASSURANCE

A.	Contractor shall be an established firm regularly engaged in satisfactory installation of similar materials and shall provide a list of 3 projects of similar nature and complexity completed in the last 5 years.  Contractor shall provide a letter of certification by manufacturer that Contractor is a current qualified installer.

- Single source responsibility:  Provide fillers, underlayments, waterproof membrane, primers, body coats and top coats produced by the same manufacturer with no less than 10 years’ experience in the manufacture and supply of principal materials for work in this section.

C.	Prior to commencing the installation, the Contractor shall install, with Owner’s approval, a mutually agreed upon sample (“mock-up”) to show final color and texture of the system.  This mock-up shall serve as a job standard for the final installation.

1.05	DELIVERY AND STORAGE

A.	Material shall be delivered to project site in manufacturer’s original unopened containers bearing manufacturer’s name, product and color.

- Materials shall be stored indoors, protected from damage, moisture, direct sunlight and temperatures below 50 degrees F or above 80 degrees F.

1.06	WARRANTY

A.	Contractor shall furnish a written warranty covering both material and workmanship for a period of one full year from the date of installation.

PART 2 PRODUCTS

2.01	MANUFACTURER

Master Builders Solutions

889 Valley Park Drive

Shakopee, MN  55379 USA

Customer Service:  800-433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Website: www.master-builders-solutions.com/en-us

2.02	MATERIALS

- MasterTop 1254 System, Decorative Floor System

- Decorative heavy-duty flooring shall be a three-component epoxy floor system consisting of epoxy resin, cure agent and specially graded aggregate troweled to a minimum thickness of 1/8 inch into which colored quartz aggregate is broadcast at a minimum thickness of 1/16 inch.  Decorative heavy-duty flooring shall be finished with a minimum two coats of clear epoxy for a minimum finished thickness of 3/16 inch.

- Physical Properties.  The Special Epoxy Flooring Systems shall comply with the following minimum test standards:

| Compressive Strength, ASTM C 579 | 12,900 psi |
| --- | --- |
| Tensile Strength, ASTM D 638 | 1,160 psi |
| Flexural Strength, ASTM D 790 | 4,600 psi |
| Indentation, MIL-D-3134 or MIL-D 24613 | 24 hrs. residual 0.00 in. |
| Impact Resistance, MIL-D-3134 or MIL-D-24613 | No chipping, cracking or delamination |
| Fire Resistance, MIL-D-3134 or MIL-D-24613 | Fire Retardant |
| Slip resistance properties, MIL-D-3134 or MIL-D-24613 | Static Friction .6 Static Friction .6 |
| Abrasion Resistance, CS17 Wheel 1000 gram load, 1000 cycles | .060 gram loss |

Where chemical resistance is a requirement, add the following, followed by the chemicals and concentrations required:

- Special flooring shall show no chemical attack when tested in accordance with ASTM D 1308 for 7 days against the following reagents and concentrations 	noted.

List chemicals here

Optional:

- MasterTop Chemical Resistant Sealer, MasterTop TC 493

- Chemical resistant aliphatic polyurethane or polyaspartic sealer applied by squeegee or trowel and roller at a minimum dry film thickness of 4 mils.

a.	Physical Properties - The chemical resistant sealer shall comply with the following minimum test standards:

| Composition | Aliphatic Polyurethane |
| --- | --- |
| Adhesion to epoxy system ASTM D 903 | 30 pli |
| Abrasion, ASTM D 4060, CS 17 wheel 1,000 cycles, 1,000 gram load | .097 grams loss |
| Moisture Vapor Transmission, ASTM E 96 | .01 perm inch |
| Accelerated weathering ASTM D 822 | No effect after 2,000 hours |

b.	Chemical Resistance. The flooring system shall show no chemical attack or discoloration when tested in accordance with ASTM D 1308 at 72 degrees F. against the following reagents and concentrations noted for 7 days.

| Reagent | Reagent |
| --- | --- |
| Acetic Acid 20% | Benzene |
| Acetone | Benzoic Acid |
| Ethylene Dichloride | Butyl Alcohol |
| Lactic Acid 50% | Citric Acid |
| Nitric Acid 10% | Diesel Fuel |
| Phenol | Stearic Acid |
| Sulfuric Acid 45% | Amyl Acetate |
| Toluene | Dichloracetic Acid |
| Trichloroethylene | Chlorobenzene |

PART 3

3.01	SURFACE CONDITIONS

A.	After concrete curing period (28 days minimum) has elapsed, surface must be clean and dry, physically sound and free of contamination.  Surfaces must be free of holes, voids, or defects.  Cracks and abrupt changes in surface profile must be corrected.  Fins and projections must be removed.  All curing compounds and sealers must be removed.

B.	Verify that moisture content is within range acceptable to flooring manufacturer, using a calcium chloride test kit in accordance with ASTM F 1869.

C.	Contractor must report, in writing, surfaces left in improper condition by other trades.  Application will constitute acceptance of surfaces by the applicator.

3.02	PREPARATION

A.	Prepare surfaces as required, per manufacturer’s printed instructions.  Preferred surface preparation is shotblast or similar mechanical method.

B.	Patch all depressions, divots, honeycombed or scaled concrete with filler as recommended by manufacturer.

C.	Level and slope floor, as required, with manufacturer’s acrylic or epoxy modified mortar underlayment.

D.	Fill all non-moving cracks or control joints with joint filler as recommended by manufacturer.

E.	Fill all moving cracks or joints with a firm but flexible (or non-rigid) sealant material as recommended by manufacturer.  Expansion joints should be re-cut in finished floor, if required, and filled with sealant.

F.	Masking:  Mask surfaces that require protection.

3.03	INSTALLATION

A.	Comply with flooring system manufacturer’s recommendation.

- Materials shall be prepared and mixed in compliance with flooring manufacturer’s instructions.

3.	Apply primer as recommended by flooring manufacturer.

4.	Trowel apply mixed material at manufacturer’s recommended rate to achieve a minimum thickness of ___ inch (1/8, 3/16, or 1/4 inch).

- Apply two coats of finish in color selected at manufacturer’s recommended rate to	achieve desired finish and texture selected.

(Optional) 	a.	As conditions require, broadcast aluminum oxide, quartz or approved aggregates into grout coat for optimum skid resistance.

- Total floor system shall be a minimum of ___ inch (1/8, 3/16, or 1/4 inch), exclusive of underlayment and waterproof membrane.

Insert the following where chemical resistant polyurethane sealer is required.

- Apply chemical resistant aliphatic polyurethane clear sealer at a minimum 4 mils dry film thickness in one application.

B.	Cove Base:  Where specified, install a (_____) inch high cove base with a nominal    1-inch radius onto wall surfaces.  All cove bases shall terminate into cap strips, unless otherwise noted on drawings.

Optional:

3.04	FIELD QUALITY CONTROL

A.	Core Sampling.  At the direction of the owner and at locations designated by the owner, take core sample to verify the thickness of the finished floor system.  Repair damage caused by coring and correct deficiencies, if found, at no additional cost to owner.

3.05	CLEANUP

A.	Remove waste materials, rubbish and debris and dispose of them in accordance with local regulations.  Leave work areas in a clean condition.

3.06	PROTECTION

A.	Protect the completed work from water, airborne particles or other surface contaminants until cured, tack free, approximately 18-24 hours after application.

B.	Protect completed system from traffic and physical abuse for approximately 72 hours.  Protect completed system from immersion and chemical exposure until thoroughly cured, approximately seven (7) days.

END OF SECTION

Disclaimer

THIS INFORMATION AND ALL FURTHER TECHNICAL ADVICE ARE BASED ON master builders solutions PRESENT KNOWLEDGE AND EXPERIENCE. HOWEVER, master builders solutions ASSUMES NO LIABILITY FOR PROVIDING SUCH INFORMATION AND ADVICE INCLUDING THE EXTENT TO WHICH SUCH INFORMATION AND ADVICE MAY RELATE TO EXISTING THIRD-PARTY INTELLECTUAL PROPERTY RIGHTS, ESPECIALLY PATENT RIGHTS. IN PARTICULAR, master builders solutions DISCLAIMS ALL CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. master builders solutions SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. master builders solutions RESERVES THE RIGHT TO MAKE CHANGES ACCORDING TO TECHNoLOGY PROGRESS OR FUrTHER DEVELOPMENTS. IT IS THE CUSTOMERS RESPONSIBILITY AND OBLIGATION TO CAREFULLY INSPECT AND TEST ANY INCOMING GOODS. PERForMANCE OF THE PRODUCT(S) DESCRIBED HEREIN SHOULD BE VERIFIED BY TESTING AND CARRIED OUT ONLY BY QUALIFIED EXPERTS. IT IS THE SOLE RESPONSIBILITY OF THE CUSTOMER TO CARRY OUT AND ARRANGE FOR ANY SUCH TESTING. REFERENCE TO TRADE NAMES USED BY OTHER COMPANIES IS NEITHER A RECOMMENDATION, NOR AN ENDORSeMENT OF ANY PRODUCT AND DOES NOT IMPLY THAT SIMILAR PRODUCT COULD OR COULD NOT BE USED.