**Adhered Veneer Surfacing for Concrete and Masonry Units**

Weather resistant surfacing system incorporating a Senergy air/water-resistive barrier and adhered veneer finish.

**INTRODUCTION**

This specification refers to application of the Senergy Adhered Veneer Surfacing over concrete and concrete masonry units (CMU) walls.

**DESIGN RESPONSIBILITY**

It is the responsibility of both the specifier and the purchaser to determine if a product is suitable for its intended use. The designer selected by the purchaser shall be responsible for all decisions pertaining to design, detail, structural capability, attachment details, shop drawings and the like. The Wall Systems business of Master Builders Solutions Construction Systems US, LLC (herein referred to as “Master Builders Solutions”) has prepared guidelines in the form of specifications, typical application details, and product bulletins to facilitate the design process only. Master Builders Solutions is not liable for any errors or omissions in design, detail, structural capability, attachment details, shop drawings or the like, whether based upon the information provided by Master Builders Solutions or otherwise, or for any changes which the purchasers, specifiers, designers or their appointed representatives may make to Master Builders Solutions published comments. The International Building Code and TMS 402/602 *Building Code Requirements and Specification for Masonry Structures* do not place a specific height limit on this application. However local building code may impose certain restrictions that would limit the height that the system can be placed. Consult the authority having jurisdiction (AHJ) for the project to ensure local requirements are satisfied.

**DESIGNING AND DETAILING A SENERGY ADHERED VENEER SURFACING SYSTEM**

General: The system shall be installed in strict accordance with current recommended published details and product specifications from the system’s manufacturer.

1. **Substrate Systems:**
2. Acceptable substrates are Concrete Masonry Units (excluding fluted block; split faced block should be assessed on project by project basis) brick and concrete walls.
3. Painted and otherwise coated surfaces should be inspected and prepared as approved by Master Builders Solutions before application. The applicator shall verify that the proposed substrate is acceptable prior to the Senergy Adhered Veneer Surfacing System installation.
4. **System Joints**
5. It is the sole responsibility of the project design team, including the architect, engineer, etc., to ultimately determine specific expansion joint placement, width and design. Detail specific locations in construction drawings.
6. Sealant joints are required at all penetrations through the Senergy System.
7. For a list of acceptable sealants refer to *Acceptable Sealants for use with Senergy Wall Systems* technical bulletin.
8. **Grade Condition:** The Senergy Surfacing System is not intended for use below grade or on surfaces subject to continuous or intermittent immersion in water or hydrostatic pressure.

**TECHNICAL INFORMATION**

Consult Master Builders Solutions’ Technical Services Department for specific recommendations concerning all other applications. Consult the Senergy website, senergy.master-builders-solutions.com, for additional information about products, systems and for updated literature.

**PART 1 GENERAL**

**NOTE TO SPECIFIER: Items in blue/underlined indicate a system option or choice of options. Throughout the specification, delete those which are not required or utilized.**

* 1. **SECTION INCLUDES**

1. Senergy products are listed in this specification to establish a standard of quality. Any substitutions to this specification shall be submitted to and receive approval from the Architect at least 10 days before bidding. Proof of equality shall be borne by the submitter.
2. Senergy Adhered Veneer Surfacing System: consisting of Senergy air/water-resistive barrier and MaxGrip Veneer Mortar.
   1. **RELATED SECTIONS**
3. Products installed, but not supplied under this section: substrate, flashing and sealant.
   1. **SUBMITTALS**
4. Submit under provisions of Section [01 33 00] [x].
5. Product Data: Provide data on Senergy Adhered Veneer Surfacing System materials, product characteristics, performance criteria, limitations and durability.
6. Certificate: System manufacturer’s approval of applicator.
7. Sealant: Sealant manufacturer’s certificate of compliance with ASTM C1382.
8. System manufacturer’s current specifications, typical details, system overview and related product literature which indicate preparation required, storage, installation techniques and jointing requirements.

* 1. **QUALITY ASSURANCE**

1. Manufacturer: More than 10 years in the industry, with more than 1000 completed projects.
2. Applicator: Approved by Master Builders Solutions in performing work of this section.
3. Regulatory Requirements: Conform to applicable code requirements resurfacing system.
4. Field Samples:
   1. Provide under provisions of Section [01 43 36] [01 43 39].
   2. Prepare each sample panel using the same tools and techniques to be used for the actual application.
   3. Locate sample panel where directed.
   4. Accepted sample panel [may] [may not] remain as part of the work.
5. Testing:
6. General Air/Water-Resistive Barrier Minimum Performance:

|  |  |  |  |
| --- | --- | --- | --- |
| **TEST** | **METHOD** | **CRITERIA** | **RESULTS** |
| Water-resistive barrier coatings used under EIFS | ASTM E2570 |  | Meets all performance requirements |
| Air Leakage of Air Barrier Assemblies | ASTM E2357 | 0.2 l/(s.m2) @75 Pa  (0.04 cfm/ft2 @ 1.57 psf) | 0.0007 l/s.m2 (0.0001 cfm/ft2) @ 75 Pa (1.57 psf) positive / post conditioning  0.0014 l/s.m2 (0.0003 cfm/ft2) @ 75 Pa (1.57 psf) negative / post conditioning |
| Air Permeance of Building Materials | ASTM E2178 | 0.02 l/(s.m2) @75 Pa  (0.004 cfm/ft2 @ 1.57 psf) | 0.0049 l/s.m2 @ 75 Pa  (0.00098 cfm/ft2 @ 1.57 psf) |
| Rate of Air Leakage | ASTM E283 |  | 0.0185 l/s·m2 @ 75 Pa (0.0037 cfm/ft2 @ 1.57 psf) |
| Water Vapor Transmission | ASTM E96 | Report value | Senershield-R - 18 Perms (grains/Hr. in Hg. ft2) @ 10 mils wet film thickness  Senershield-RS 18 Perms (grains/Hr. in Hg. ft2) @ 12 mils wet film thickness  Senershield-R/RS - 14 Perms (grains/Hr. in Hg. ft2) @ 20 mils wet film thickness  Senershield-VB - 0.09 Perms (grains/Hr. in Hg. ft2) @ 26 mils wet film thickness |
| Pull-Off Strength of Coatings | ASTM D4541 | Min. 110 kPa (15.9 psi) or substrate failure | Pass - Tested over exterior gypsum sheathing, ASTM C1177 glass-mat sheathing, cement board, OSB, plywood; pvc and galvanized flashing |
| Nail Sealability (without Sheathing Fabric) | ASTM D1970 | No water penetration at galvanized roofing nail penetration under 127 mm (5”) head of water after 3 days at 4° C (40° F) | Pass |
| Surface Burning | ASTM E84 | Flame Spread < 25  Smoke Development < 450 | Meets Class A: Flame spread =15  Smoke developed = 95 |

1. Air/Water-Resistive Barrier ICC-ES AC-212:

|  |  |  |  |
| --- | --- | --- | --- |
| **TEST** | **METHOD** | **CRITERIA** | **RESULTS** |
| Sequential Testing:   1. Structural 2. Racking 3. Restrained Environmental Conditioning 4. Water Penetration | 1. ASTM E 1233 Procedure A 2. ASTM E 72 3. ICC-ES AC-212 4. ASTM E 331 | No cracking at joints or interface of flashing  No water penetration after 15 min @ 137 Pa (2.86 psf) | Pass - Tested over OSB and gypsum sheathing  No water penetration after 90 min @ 299 Pa (6.24 psf) |
| Sequential Testing:   1. UV Light Exposure 2. Accelerated Aging 3. Hydrostatic Pressure Test | 1. ICC-ES AC-212 2. ICC-ES AC-212 3. AATCC 127-1985 | No cracking or bond failure to substrate  No water penetration after 21.7 in (550 mm) water for 5 hours | Pass |
| Freeze-Thaw | ASTM E 2485 (Method B) | No sign of deleterious effects after 10 cycles | Pass - Tested over exterior gypsum sheathing, ASTM C1177 glass-mat sheathing, cement board, OSB, plywood |
| Water Resistance | ASTM D2247 | No deleterious effects after 14 day exposure | Pass - Tested over exterior gypsum sheathing, ASTM C1177 glass-mat sheathing, cement board, OSB, plywood |
| Tensile Bond | ASTM C 297 | Minimum 103 kPa (15 psi) | Pass - Tested over exterior gypsum sheathing, ASTM C1177 glass-mat sheathing, cement board, OSB, plywood, CMU; pvc and galvanized flashing |
| Tensile Bond (after freeze-thaw) | ASTM C 297 | Minimum 103 kPa (15 psi) avg; no failure after 10 cycles freeze-thaw | Pass |

1. Air/Water-Resistive Barrier ICC-ES AC 148:

|  |  |  |  |
| --- | --- | --- | --- |
| **TEST** | **METHOD** | **CRITERIA** | **RESULTS** |
| Sequential Testing:   1. UV Light Exposure 2. Accelerated Aging 3. Hydrostatic Pressure Test | 1. ICC-ES AC 148 2. ICC-ES AC 148 3. AATCC 127-1985 | No cracking or bond failure to substrate  No water penetration after 21.7 in (550 mm) water for 5 hours | Pass |
| Peel Adhesion | ASTM D 3330 Method F | After UV Exposure  After Accelerated Aging  After Elevated Temperature Exposure  After Water Immersion | Pass - tested over ASTM C1177 glass-mat sheathing, OSB, plywood, PVC and uncoated aluminum |
| Nail Sealability after Thermal Cycling | ASTM D 1970 (Modified), AAMA 711 | No water penetration at galvanized roofing nail penetration under 31 mm (1.2”) head of water after 24 hours at 4° C (40° F) | Pass |
| Tensile Strength after UV Exposure | ASTM D 5034, AAMA 711 | Minimum 0.5 N/mm (2.9 lbs/in) | Pass |
| Cold Temperature Pliability | ASTM D 1970, AAMA 711 | No cracking after bending around a 25 mm (1”) mandrel after 2 hour exposure to -18° C (0° F) | Pass |
| Resistance to Peeling | AAMA 711 | No signs of distress or failure after 24 hours of exposure at room temperature, 50° C (122° F), 65° C (149° F), 80° C (176° F) | Pass |

1. MAXGRIP VENEER MORTAR:

|  |  |  |  |
| --- | --- | --- | --- |
| **TEST** | **METHOD** | **CRITERIA** | **RESULTS** |
| Compressive Strength | ASTM C 109 | N/A | 4000 psi |
| Freeze-Thaw | ASTM C 666 | Procedure A- cycles rapid freezing and thawing in water. 40°F - 0°F - 40°F in not less than 2 hours and not more than 5 hours;  modified using full IVS composite in place of concrete beam | > 100 cycles, no failure of MaxGrip |
| Shear Strength | ANSI 118.4 | 28 days ≥ 200 psi  After 7 day water immersion ≥ 150 psi | 565 psi at 28 days  306 psi after 7 day water immersion |
| Shear Strength | ANSI A118.15 | 7 days ≥ 300 psi  28 days ≥ 400 psi  After 7 days water immersion ≥ 200 psi | 487 psi at 7 days  565 psi at 28 days  306 psi after 7 day water immersion |
| Shear Bond | ASTM C482 | Minimum 50 psi | 130 psi - Directly to molded cement mortar bed specified in ASTM  151 psi and 141 psi respectively - to Senergy Alpha Base Coat and Alpha Dry Base Coat over molded cement mortar bed specified in ASTM C482. |

* 1. **DELIVERY, STORAGE AND HANDLING**

1. Deliver, store and handle products under provisions of Section [01 66 00] [ ].
2. Deliver Senergy materials in original unopened packages with manufacturer’s labels intact.
3. Protect Senergy materials during transportation and installation to avoid physical damage.
4. Store Senergy materials in cool, dry place protected from freezing. Store at no less than 40°F/4°C.
5. Store Senergy Reinforcing Mesh in cool, dry place protected from exposure to moisture.
   1. **SEQUENCING AND SCHEDULING**
6. Coordinate and schedule installation of Senergy Adhered Veneer Surfacing System with related work of other sections.
7. Coordinate and schedule installation of trim, flashing, and joint sealers to prevent water infiltration behind the existing system.
8. Coordinate and schedule installation of windows, doors, A/C units, air seals etc. if being removed and replaced.
   1. **PROJECT/SITE CONDITIONS**
9. Existing conditions: The contractor shall refer to Section 02 00 00 for project requirements and this contractor’s responsibility there under.
10. Do not apply Master Builders Solutions materials in ambient temperatures below 40°F/4°C. Provide properly vented, supplementary heat during installation and drying period when temperatures less than 40°F/4°C prevail.
11. Do not apply Master Builders Solutions materials to frozen surfaces.
12. Maintain ambient temperature at or above 40°F/4°C during and at least 24 hours after Master Builders Solutions material installation and until dry.
13. Protect applied Master Builders Solutions materials from rain for 24 hours or until dry.

* 1. **WARRANTY**

1. Provide Master Builders Solutions material warranty for the Adhered Veneer Surfacing System installations under provisions of Section [01 07 00].
2. Comply with Senergy application instructions and notification procedures to assure qualification for warranty.

**PART 2 - PRODUCTS**

* 1. **MANUFACTURERS**

1. Senergy Adhered Veneer Surfacing System manufactured by Master Builders Solutions.
   1. **MATERIALS**

**(NOTE TO SPECIFIER: Items in blue/underlined indicate a system option or choice of options. Throughout the specification, delete those which are not required or utilized. Contact Master Builders Solutions’ Technical Service Department for further assistance.)**

1. **Air/water-Resistive Barrier Components:**
   * + 1. WS FIL Block Filler: A one-component, water-based block filler designed to prepare rough, porous concrete /masonry substrates for subsequent application of Senergy fluid applied air/water-resistive barrier products
       2. Air/Water-Resistive Barrier: ***(Required, Select a, b or c)***
       3. [SENERSHIELD-R](http://www.senergy.basf.com/en/products/Air_Water_ResistiveBarriersDrainage/Pages/Senershield-R.aspx): A one-component fluid-applied vapor permeable air/water-resistive barrier.
       4. SENERSHIELD-RS: A one-component fluid-applied vapor permeable air/water-resistive barrier for use with airless spray equipment.
       5. SENERSHIELD-VB: A one-component fluid-applied vapor impermeable air/water-resistive barrier.
       6. Rough Opening and Joint Treatment: **(Required for rough openings if wood blocking is present, select a or b)**
2. SHEATHING FABRIC: A spun-bonded non-woven reinforced polyester web for use with Senergy fluid applied air/weather-resistive barriers.
3. MAXFLASH: A one-component elastomeric material for use as a flexible flashing membrane.
   * + 1. Transitional Membrane / Expansion Joint Flashing **(If selected, both a & b are required)**
4. WS FLASH: 30-mil thick, self-sealing, self-healing composite membrane of polyester fabric and rubberized asphalt. Compatible with Senergy liquid air/weather resistive barriers.
5. FLASHING PRIMER: A water-based primer for use prior to application of WS FLASH on all acceptable surfaces.
   * + 1. Cold Temperature Additive:
6. LT ADDITIVE: Blending of LT ADDITIVE with a pail of SENERSHIELD-R/-RS/-VB enables application of these materials at temperatures as low as 25°F (-4°C).
7. **MaxGrip Veneer Mortar:** A high-strength specially formulated adhesive used to fasten manufactured stone, ceramic tile and thin brick
8. **Adhered Veneer (By Other):**
   1. Manufactured Stone Veneer Units: shall comply with ICC-ES AC51 Acceptance Criteria Adhered Manufactured Stone Masonry Veneer or ASTM C1670 Standard Specification for Adhered Manufactured Stone Masonry Veneer Units.
   2. Thin Brick Veneer Units: shall comply with ASTM C1088 Standard Specification for Thin Veneer Brick Units Made from Clay or Shale.
   3. Tile: shall comply with requirements of the Tile Council of North America/ANSI A137.1 Standard for Ceramic Tile and other applicable TCNA standards.

**PART 3 - EXECUTION**

* 1. **EXAMINATION**

1. Examine surfaces to receive Senergy Adhered Veneer Surfacing System and verify that substrate and adjacent materials are dry, clean, cured, sound and free of releasing agents, paint, or other residue or coatings. Verify substrate surface is flat, free of fins or planar irregularities greater than 1/4" in 10' (6.4 mm in 3 m).
2. Ensure adhesion tests meet the requirements listed in the *Basics of Conducting Adhesion Testing Senergy* technical bulletin.
3. Fill large voids and irregularities with appropriate parging or cement mortar materials.
4. Control/Expansion joint type and placement shall be the responsibility of the architect/engineer and substrate manufacturer.
5. Unsatisfactory conditions shall be reported to the general contractor and corrected before application of the Senergy Adhered Veneer Surfacing System.
   1. **PREPARATION**
6. All surfaces to receive Senergy Adhered Veneer Surfacing System components must be clean, dry and free of airborne contaminants.
7. Protect all surrounding areas and surfaces from damage and staining during application of Senergy Adhered Veneer Surfacing System.
8. Protect finished work at end of each day to prevent water penetration.
   1. **MIXING**

General: No additives are permitted unless specified in product mixing instructions. Close containers when not in use. Prepare in a container that is clean and free of foreign substances. Do not use a container which has contained or been cleaned with a petroleum-based product. Clean tools with soap and water immediately after use.

**NOTE TO SPECIFIER: Keep only the products in this section which were selected in Section 2.02. Delete those not to be utilized.**

1. **Air/Water-Resistive Barriers:**
2. WS FIL & SENERSHIELD-R/RS/VB: Mix with a clean, rust-free paddle and drill until thoroughly blended. Do not add water.
3. Cold Temperature Additive: LT ADDITIVE: Pour the entire contents of one (1) bottle of LT ADDITIVE into one (1) full pail of SENERSHIELD-R/RS/VB. Mix with a clean, rust-free paddle and drill until fully blended.
4. **MAXGRIP VENEER MORTAR:**
   * + - 1. Skim Coat: Prepare to mix one bag in a 5-gallon (19-liter) pail that is clean and free of foreign substances. 1.0 - 1.25 gallons (3.8 - 4.7 liters) of clean, potable water to a pail. Add a full bag of MAXGRIP VENEER MORTAR to the pail in small increments, mixing after each addition. Mix with a low speed drill with a 4-sided mortar paddle until thoroughly blended. Let stand for 5 to 10 minutes, then remix/retemper for 1 minute before use.
         2. Light Weight Adhered Veneer such as Thick Brick: Prepare to mix one bag in a 5-gallon (19-liter) pail that is clean and free of foreign substances. Add 1.0 - 1.25 gallons (3.8 - 4.7 liters) of clean, potable water to a pail. Add a full bag of MAXGRIP VENEER MORTAR to the pail in small increments, mixing after each addition. Mix with a low speed drill with a 4-sided mortar paddle until thoroughly blended. Additional water may be added to adjust workability, do not exceed 1.25 gallons. Let stand for 5 to 10 minutes, then remix / retemper for 1 minute before use. The mixed material should have a thick putty consistency and not slide off the trowel when held vertically.
         3. Heavy Stone and Tile: Prepare to mix one bag in a 5-gallon (19-liter) pail that is clean and free of foreign substances. Add 0.75 - 1.0 gallons (2.8 - 3.8 liters) of clean, potable water to a pail. Add a full bag of MAXGRIP VENEER MORTAR to the pail in small increments, mixing after each addition. Mix with a low speed drill with a 4-sided mortar paddle until thoroughly blended. Additional water may be added to adjust workability, do not exceed 1 gallon. Let stand for 5 to 10 minutes, then remix / retemper for 1 minute before use. The mixed material should have a thick putty consistency and not slide off the trowel when held vertically.
   1. **APPLICATION**

**NOTE TO SPECIFIER: Keep only the products in this section which were selected in Section 2.02. Delete those not to be utilized.**

1. **Air/Water-Resistive Barriers:**
2. Windows/openings must be protected, and the air/water-resistive barrier applied in accordance with Air/Water-Resistive/Vapor Barrier Application Guideline technical bulletin.
3. Substrate shall be dry, clean, sound, and free of releasing agents, paint, or other residue or coatings. Verify substrate is flat, free of fins or planar irregularities greater than ¼" in 10' (6.4 mm in 3 m).
4. Unsatisfactory conditions shall be corrected before application of the Senergy air/water-resistive barriers.
5. Apply the SHEATHING FABRIC and Senergy air/water-resistive barrier in accordance with the Senergy air/water-resistive barrier product bulletin.
6. Apply the MAXFLASH in accordance with the product bulletin.
7. Installed materials shall be checked before continuing system application.
8. **MAXGRIP – ADHERED VENEER MORTAR:**

**Note: MAXGRIP shall be applied and veneer installed such that the MAXGRIP is free of voids. Allow MAXGRIP to cure for 24-hours before applying pointing mortar.**

Prior to installing the adhered veneer, apply selected MAXGRIP VENEER MORTAR as a skim coat over cement board sheathing at approximately 1/6” (1.6mm) thick. Apply to an area that can be covered with adhered veneer before the skim coat dries. Allow smit coat layer to set for 3-5 minutes, then proceed with adhering the selected veneer

1. Thin brick veneer: Spread MAXGRIP VENEER MORTAR onto the back of bricks in a continuous layer nominally 3/16” to ¼” (5 - 6mm) thick and press bricks firmly into place on the substrate.
2. Stone veneer: Apply MAXGRIP VENEER MORTAR to the back of clean stone veneer in a continuous layer nominally ¼” to 3/8” (6 - 9mm) thick. Press firmly in place with a twisting movement until excess material exudes from the sides of the unit. Remove excess MAXGRIP VENEER MORTAR between units.
3. Tile: Apply MAXGRIP VENEER MORTAR as a skim coat over cement board at approximately 1/16” (1.6mm) thick. Apply only to an area that can be covered with tile before the MAXGRIP VENEER MORTAR skim coat dries. Installation should proceed in accordance with ANSI A 108.5 (the type and size of the tile will dictate adhesive application.)

**3.05 CLEANING**

* + - * 1. Clean work under provisions of Section [01 74 00] [x].
        2. Clean adjacent surfaces and remove excess material, droppings, and debris.

**3.06 PROTECTION**

* + 1. Protect Master Builders Solutions materials from rain and temperatures below 40°F (4°C) for 24 hours or until dry.
    2. Protect installed construction under provisions of Section [01 76 00] [ ].

**END OF SECTION**

**Warranty**

Master Builders Solutions Construction Systems US, LLC (hereinafter “Master Builders Solutions”) warrants this product to be free from manufacturing defects and to meet the technical properties on the current Product Bulletin, if used as directed within shelf life. Satisfactory results depend not only on quality products but also upon many factors beyond our control. MASTER BUILDERS SOLUTIONS MAKES NO OTHER WARRANTY OR GUARANTEE, EXPRESS OR IMPLIED, INCLUDING WARRANTIES OF MERCHANTABILITY OR FITNESS FOR A PARTICULAR PURPOSE WITH RESPECT TO ITS PRODUCTS. The sole and exclusive remedy of Purchaser for any claim concerning this product, including but not limited to, claims alleging breach of warranty, negligence, strict liability or otherwise, is shipment to purchaser of product equal to the amount of product that fails to meet this warranty or refund of the original purchase price of product that fails to meet this warranty, at the sole option of Master Builders Solutions. In the absence of an extended warranty issued by Master Builders Solutions, any claims concerning this product must be received in writing within one (1) year from the date of shipment and any claims not presented within that period are waived by Purchaser. Master Builders Solutions WILL NOT BE RESPONSIBLE FOR ANY SPECIAL, INCIDENTAL, CONSEQUENTIAL (INCLUDING LOST PROFITS) OR PUNITIVE DAMAGES OF ANY KIND.

Purchaser must determine the suitability of the products for the intended use and assumes all risks and liabilities in connection therewith. This information and all further technical advice are based on Master Builders Solutions’ present knowledge and experience. However, Master Builders Solutions assumes no liability for providing such information and advice including the extent to which such information and advice may relate to existing third party intellectual property rights, especially patent rights, nor shall any legal relationship be created by or arise from the provision of such information and advice. Master Builders Solutions reserves the right to make any changes according to technological progress or further developments. The Purchaser of the Product(s) must test the product(s) for suitability for the intended application and purpose before proceeding with a full application of the product(s). Performance of the product described herein should be verified by testing and carried out by qualified experts.