SECTION 09 67 23

UCRETE® UD200 SR

Note to specifiers:

The purpose of this guide specification is to assist the specifier in developing a project specification for the use of BASF Corporation products.  it is not intended to be a “stand alone” document, nor to be copied directly into a project manual.  This guide specification will need to be carefully reviewed for APPROPRIATENESS for the given project and edited accordingly to comply with project-specific requirements.

PART 1 GENERAL

1.01	WORK INCLUDED:

- Provisions established within the Contract, Division 1, General Requirements, the Drawings are collectively applicable to this Section.

- Related sections Section 09 77 00 Special Protective Wall Coatings.

1.02	Products installed but not furnished under this section

- Division 3: Concrete (poured in place).

- Division 7: Sealants: Control joints, expansion joints and doorframes.

- Division 15: Mechanical: Drains

1.03	REFERENCE STANDARDS

- American Society for Testing and Materials (ASTM)

1.04	SUBMITTALS:

- Prior to commencing work, submit Manufacturer’s technical information and installation details to describe materials to be used.  The same Manufacturer shall supply all polymer underlayments, wall and floor finishes.

- LEED Submittals:  Comply with requirements for each product to achieve points indicated in LEED Project Checklist provided by the Architect/Engineer.

- Submit Manufacturer’s certificate of compliance that materials meet specification requirements.

- Before beginning work, samples of the flooring system shall be provided for Architect/Engineer’s approval.

1.05	QUALITY ASSURANCE:

- Contractor shall be an established firm regularly engaged in satisfactory installation of similar materials for the past 5 years.  Contractor shall provide a letter of certification by Manufacturer that Contractor is a current qualified installer.

- Single source responsibility: Provide fillers, broadcast media, underlayments, polyurethane body coat produced by the same manufacturer with no less than 15 years’ experience in the manufacture and supply of these principal materials for work in this section.

- Manufacturer Qualifications: Company shall be ISO 9001: 2015 Certified

- Verification must be supplied by the Manufacturer that the polyurethane concrete-based flooring system has passed, with an Observed Growth Rating of one (1), ASTM G 21-90: Standard Practice for Determining Resistance of Synthetic Polymeric Materials to Fungi.  This result will ensure that the polyurethane concrete-based flooring system will not support the growth of hazardous fungi.

- Verification must be supplied by the manufacturer that the polyurethane concrete-based flooring system has passed, ASTM G 22-76: Standard Practice for Determining Resistance of Plastics to Bacterial, Procedure B.  No evidence of E.coli or Salmonella choleraesuis growth should be observed.

- Owner and Contractor shall review and mutually agree upon color, grade and final texture and chemical-resistant of the polyurethane composite floor system before starting installation.

- Prior to commencing the installation, the Contractor shall install, with Owner’s approval, a mutually agreed upon sample (“mock-up” 10’ by 10’) to show final color and texture of the system.  This mock-up shall serve as a job standard for the final installation.

1.06	DELIVERY AND STORAGE:

- Material shall be delivered to project site in Manufacturer’s original unopened containers bearing manufacturer’s name, product and color.

- Comply with Manufacturer’s ordering instructions and lead-time requirements to avoid construction delays.

- Materials shall be stored indoors, protected from damage, moisture, direct sunlight and temperatures below 50°F (10°C) or above 80°F (27°C).

1.07	PROJECT CONDITIONS

- Evaluate the substrate condition, including moisture content and extent of substrate leveling and repairs required, if any.

- Coordinate flooring work with other trades to ensure adequate illumination, ventilation, and dust free environment during application and curing of flooring.

- Comply with material Manufacturer’s recommended temperature limitations for flooring application.

1.08	WARRANTY:

- Contractor shall furnish a written warranty covering both material and workmanship for a period of one (1) year from date of installation.

PART 2 PRODUCTS

2.01	MANUFACTURER:

BASF Corporation Construction Systems

889 Valley Park Drive

Shakopee, MN  55379

Customer Service:  800-433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Internet: www.master-builders-solutions.basf.us

2.02	MATERIALS:

- UCRETE 200 SR and Ucrete RG (cove base) Slip Resistant Polyurethane Concrete Flooring system comprised of trowel-applied single base coat at ___” thickness, pigmented to agreed upon color.

2.03	PHYSICAL PROPERTIES:

- Flooring system shall comply with the following requirements:

Property				Test Standard		Result

Compressive Strength			ASTM C-579 		7,098 psi

Tensile Strength			ASTM C-307		833 psi

Flexural Strength			ASTM C-580		1,696 psi

Density					ASTM C-905		130.47 lb./ft3

Water Absorption			ASTM C-413		< 0.1%

Resistance to Fungi Growth		ASTM G-21		Observed Growth - 1

Property				Test Standard		Result

Service Temperature						-40oF to 302oF

*varies by system thickness						(-40oC to 150oC)

Impact Resistance			ASTM D-2794		160 inch-pound / Pass

Slip Resistance, Static 			ANSI/NFSI B101.1-2009 0.97 Mμ

Slip Resistance, Dynamic		ANSI/NFSI B101.3-2012 0.86 Mμ

- Flooring system shall show no chemical attack when tested in accordance with ASTM D-1308 at ambient temperature for 28 days immersion against the following reagent and concentrations noted.

Reagent	 		Reagent			Reagent

## Boric Acid 100% 		Phosphoric Acid 80%		Chlorobenzene All

Acetic Acid 20%		Ethylene Glycol 100%		Fatty Acid 100%	Hydrochloric Acid 35%	 	Ethylene Dichloride All		Glycolic 100%

Sodium hypochlorite 27%	Maleic Anhydride 100%		Picric 5%

Citric Acid 40%			Lactic Acid 85%			Benzene 100%

Copper Sulfate (in solution)	Nitric Acid 30%			Diesel Fuel 100%

Muriatic Acid 35%		Benzoic Acid 100%		Stearic Acid All

Sulfuric Acid 30% 		Butyl Alcohol 100%		Amyl Acetate All

# PART 3 EXECUTION

3.01	SURFACE CONDITIONS:

A.	Concrete must have a 7-day minimum curing period. The surface must be clean and dry, physically sound and free of contamination.  Surfaces must be free of holes, voids or defects. Cracks and abrupt changes in surface profile must be corrected. All curing compounds and sealers must be removed.

B.	Verify that moisture content is within range acceptable to Manufacturer using calcium chloride test kit in accordance with ASTM F-1869. Alternatively, ASTM F2170 can be used to determine the Relative Humidity within the concrete substrate.

C.	Contractor must report, in writing, surfaces left in improper condition by other trades.  Application will constitute acceptance of surfaces by the applicator.

PREPARATION:

- Prepare surfaces by shotblast or similar mechanical method, as recommended by manufacturer.

- Patch all depressions, divots, honeycombed or scaled concrete with polyurethane concrete filler, as recommended by manufacturer.

- Fill all static (non-moving) cracks or control joints, greater than 28 days old, with polyurethane concrete, as recommended by manufacturer.

- All control joints less than 28 days old must be re-cut and honored through flooring system, filled with control joint filler.

- Fill all active (moving) cracks or joints with a firm but flexible (or non-rigid) sealant material, as recommended by Manufacturer.  Expansion joints should be re-cut in finished floor and filled with elastomeric joint sealant.

- Saw cut a groove in the concrete (key in) at all free edges around perimeters, along channels or expansion joints, at doorways and columns, with a depth and width equal to twice the thickness of the flooring system.

3.03	PRIMING:

A. 	A primer is not normally required. However, a primer would be beneficial on very porous substrates and where hygiene, ease of cleaning and appearance are important.

3.04	INSTALLATION:

- Comply with flooring system Manufacturer’s recommendations.

1.	Mix component polyurethane concrete flooring system according to manufacturer’s instructions. UD200 SR is best mixed in a forced action mixer, such as a Mixall Kol M-61.

- Temperature requirements: site / substrate 40°– 86°F (5°-30°C), material temps 60° – 68° F (15°-20°C) (mix temp below 60°F (15°C) will make application more difficult and careful consideration should be given to storage of materials in cold conditions).

- Spread the mix evenly over the substrate and close using a steel trowel (avoid over troweling as this will result in gloss variations and impaired slip resistance) Install to a thickness of ¼” to ½” (6-12mm) depending on requirements.

- Using a short nap roller, back roll over the surface (an adhesive roller is recommended. This will provide a more even finish. This is best done immediately after troweling. The roller should be passed over the surface no more than 2 times. The roller will not flatten the surface of a poorly troweled floor.

- Do not back roll into partially cured material as this will show in the finished floor. Avoid excessive buildup of resin on the roller by rolling out immediately in front of the wet front, or on a piece of cardboard.

- Cove Base: Where specified, install a (  ”) high integral cove base with a nominal 1” radius onto wall surfaces.    Follow the standard Ucrete construction details for cove terminations.

3.05	FIELD QUALITY CONTROL - Optional

- Core Sampling.  At the direction of the owner and at locations designated by the owner, take core sample to verify the thickness of the finished floor system.  Repair damage caused by coring and correct deficiencies, if found, at no additional cost to owner.

3.06	CLEANUP

- Remove waste materials, rubbish and debris and dispose of them in accordance with local regulations.  Leave work areas in a clean condition.

  - PROTECTION:

- Protect the completed Ucrete UD 200 SR flooring system from water, airborne particles or other surface contaminates until cured and tack free, approximately (12) twelve hours at 70°F after application, or until all other trades on the construction project are completed with their project work.

- Protect completed system from full chemical exposure until thoroughly cured, approximately 7 days at 72°F.

- Protect polyurethane composite flooring from UV light which may cause a change in color hue but will not affect the physical properties of the system.

## END OF SECTION

Disclaimer.

THIS INFORMATION AND ALL FURTHER TECHNICAL ADVICE ARE BASED ON BASF’s PRESENT KNOWLEDGE AND EXPERIENCE. HOWEVER, BASF ASSUMES NO LIABILITY FOR PROVIDING SUCH INFORMATION AND ADVICE INCLUDING THE EXTENT TO WHICH SUCH INFORMATION AND ADVICE MAY RELATE TO EXISTING THIRD-PARTY INTELLECTUAL PROPERTY RIGHTS, ESPECIALLY PATENT RIGHTS. IN PARTICULAR BASF, DISCLAIMS ALL CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. BASF SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. BASF RESERVES THE RIGHT TO MAKE CHANGES ACCORDING TO TECHNILOGY PROGRESS OR FUTHER DEVELOPMENTS. IT IS THE CUSTOMERS RESPONSIBILITY AND OBLIGATION TO CAREFULLY INSPECT AND TEST ANY INCOMING GOODS. PERFROMANCE OF THE PRODUCT(S) DESCRIBED HEREIN SHOULD BE VERIFIED BY TESTING AND CARRIED OUT ONLY BY QUALIFIED EXPERTS. IT IS THE SOLE RESPONSIBILITY OF THE CUSTOMER TO CARRY OUT AND ARRANGE FOR ANY SUCH TESTING. REFERENCE TO TRADE NAMES USED BY OTHER COMPANIES IS NEITHER A RECOMMENDATION, NOR AN ENDORSMENT OF ANY PRODUCT AND DOES NOT IMPLY THAT SIMILAR PRODUCT COULD OR COULD NOT BE USED.