# SECTION 03 05 00

## INTEGRAL WATERPROOFING

GENERAL

SECTION INCLUDES

Section includes materials and procedures for integral waterproofing of concrete.

RELATED SECTIONS

** NOTE TO SPECIFIER **

Delete Sections that are not required.

- Section 01 10 00 - Summary

- Section 01 33 00 - Submittal Procedures

- Section 01 45 00 - Quality Control

- Section 01 60 00 - Product Requirements

- Section 03 10 00 - Concrete Forming and Accessories

- Section 03 30 00 - Cast-in-Place Concrete

- Section 03 31 26 - Self-Consolidating Concrete

- Section 03 35 00 - Concrete Finishing

- Section 03 39 00 - Concrete Curing

REFERENCES

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section; add others as required. Standards listed here shall be the most current ones.

ASTM International (ASTM):

    - ASTM C39/C39M - Standard Test Method for Compressive Strength of Cylindrical Concrete Specimens

    - ASTM C94/C94M - Standard Specification for Ready-Mixed Concrete

    - ASTM C494/C494M - Standard Specification for Chemical Admixtures for Concrete

American Concrete Institute (ACI):

1.	ACI SPEC-301 - Specifications for Concrete Construction

2. 	ACI SPEC-301M - Specifications for Concrete Construction (Metric)

3. 	ACI SPEC-305.1 - Specification for Hot Weather Concreting

4. 	ACI SPEC-306.1 - Standard Specification for Cold Weather Concreting

5.	ACI SPEC-308.1 - Standard Specification for Curing Concrete

NSF International (NSF):

1.	NSF/ANSI Standard 61 - Drinking Water System Components

D.	DIN (Deutsches Institut Fur Normung, Germany):

DIN 1048 Part 5 Testing Concrete – Testing of hardened concrete (specimens prepared in mould)

DIN EN 12390-8 Testing hardened concrete – Part 8: Depth of penetration of water under pressure

E.	Corps of Engineers:

1.	CRD-C 48 - Standard Test Method for Water Permeability of Concrete

SUBMITTALS

    - Submit under provisions of Section 01 33 00 Submittal Procedures.

    - Product Data:  Manufacturer's data sheet of waterproofing admixture to be used.

    - Manufacturer's Certificate: Certificate showing the conformance of admixtures to 	specified performance requirements.

QUALITY ASSURANCE

### Provide products from one manufacturer.

### A meeting shall be held two weeks prior to placement of concrete to discuss the Project and materials. Waterproofing admixture Manufacturer's Representative shall be present at the meeting.

### Conform to ACI SPEC-305.1 for hot weather concrete placement and protection.

### Conform to ACI SPEC-306.1 for cold weather concrete placement and protection.

- PRODUCTS

  - MANUFACTURER

    - Master Builders Solutions, 23700 Chagrin Blvd., Cleveland, OH 44122. Telephone: (800) 628-9990. Fax: (216) 839-8821. Web address: https://www.master-builders-solutions.com/en-us

  - WATERPROOFING ADMIXTURE (PERMEABILITY-REDUCING ADMIXTURE)

** NOTE TO SPECIFIER ** NSF Certification may be required for potable water tanks. Delete if it is not required for the project.

    - Shall be a portland cement-based crystalline capillary waterproofing admixture that reacts in concrete to form non-soluble crystalline hydration products in the capillary pores of the concrete.

    - Shall conform to ASTM C494/C494M, Type S.

    - Shall satisfy the following requirements, when used at the manufacturer’s 	recommended dosage:

- Shall show a reduction in permeability of concrete compared to an identical concrete mixture without the admixture, when tested in accordance with CRD-C 48 at a pressure of 200 psi (1.4 MPa) (equivalent to 460 ft (140 m) of head).

- Shall reduce or have no penetration of water compared to an identical concrete mixture without the admixture, when tested in accordance with DIN 1048 [EN 12390] for a duration of 72 hours.

- Shall be certified to NSF/ANSI 61.

    - Product: MasterLife 300 Series as manufactured by Master Builders Solutions.

    - Substitutions: Not permitted.

- EXECUTION

  - BATCHING, MIXING AND TRANSPORTING

### Waterproofing admixture shall be batched at the concrete production plant in a manner similar to that for cement and other cementitious materials.

### Batching and mixing of materials shall be in accordance with ASTM C94/C94M.

C.	Mix for at least for 5 minutes after the addition of waterproofing admixture.

  - PLACING, CONSOLIDATION AND FINISHING

### Placing, consolidation and finishing of concrete shall be in accordance with ACI SPEC-301 [ACI SPEC-301M].

  - COLD WEATHER CONCRETING

A. 	Concrete shall be placed and protected in accordance with ACI SPEC-306.1.

  - HOT WEATHER CONCRETING

    - Concrete shall be placed and protected in accordance with ACI SPEC-305.1.

  - CURING AND PROTECTION

### Curing and protection of concrete shall be in accordance with Section 03 39 00 [ACI SPEC-308.1].

END OF SECTION

# Text boxes

For more information, contact Master Builders Solutions; 23700 Chagrin Blvd., Beachwood, OH 44122; Phone: (800) 628-9990; Website: https://www.master-builders-solutions.com/en-us/support-for-professionals/technical-service/specifications

Options are provided in square brackets. Delete those that are not necessary.

To see the hidden notes to specifier, press Show/Hide feature ¶